GEOTECHNICAL ASSESSMENT OF TERNARY BLENDED MIXTURE FOR STABILIZATION OF CLAY SUB - GRADE

BY

IKHARIA ABDUL-HAPHIZ TEMIDAYO			2005001083

AKINYEYE TOLULOPE EMMANUEL			2005001043

OLORUNMOLA JOSHUA OLAMIDE			2005001121

AKINOKUN DANIEL AKINNIYI			2005001037

A PROJECT SUBMITTED TO THE

DEPARTMENT OF CIVIL ENGINEERING,

FACULTY OF ENGINEERING,

EKITI STATE UNIVERSITY, EKITI STATE, NIGERIA

IN PARTIAL FULFILMENT OF THE REQUIREMENT FOR THE AWARD OF BACHELOR OF ENGINEERING (B.ENG.) IN CIVIL ENGINEERING.

FEBRUARY, 2026.

# DECLARATION

We hereby declare that this project is an original work prepared and documented by us and has not been presented wholly or partially for the award of a degree elsewhere. All the citations, sources of information are acknowledged by the references incorporated.

# CERTIFICATION

This is to certify that this project report on ‘GEOTECHNICAL ASSESSMENT OF TERNARY BLENDED MIXTURE FOR STABILIZATION OF CLAY SUB – GRADE’ was prepared and submitted by IKHARIA ABDUL-HAPHIZ TEMIDAYO, OLORUNMOLA JOSHUA OLAMIDE, AKINOKUN DANIEL AKINNIYI and AKINYEYE TOLULOPE EMMANUEL to The Department of Civil Engineering Faculty of Engineering, Ekiti State University, Ado-Ekiti. The Project has been read and approved as meeting the requirement of the department for the Bachelor of Engineering (B.Eng.) Degree.

_____________________				_________________________

Engr. B. A. ALO					                      Date

Supervisor

_______________________			            ___________________________

Prof. O. O. Aluko		        				          Date

Head of Department

# DEDICATION

This project is dedicated to God Almighty who has given me the privilege to be a part of this, and also for His grace and favor during my study. He alone deserves the praise, right from the beginning till this moment even until the completion of this course, I give Him glory for His mercies.

# ACKNOWLEDGEMENT

I thank the Almighty God for His mercies which endured forever over my life and how His love has been holding me through. Also, for the strength which He has given me to complete this program at Ekiti State University.

My profound gratitude goes to my supervisor Engr. B. A. ALO for his love and concern as a teacher and mentor. This work could not have been complete without his support, tolerance, efforts, and understanding in going through my manuscripts and naming necessary corrections, helping to ensure this project became the best it could be. I am very grateful sir.

My appreciation goes to all my lecturers in the Civil Department, and laboratory attendance who have also contributed to this project, especially my project supervisor, Engr. B. A. ALO. I will eternally be grateful for good deeds sir.

ABSTRACT

Laboratory tests were conducted on both untreated and stabilized soil samples in accordance with relevant British Standards. The experimental program included grain size distribution, Atterberg limits, compaction characteristics, unconfined compressive strength (UCS), California Bearing Ratio (CBR). A total of 12 mix proportions were considered to determine the optimum combination that would provide the best overall performance. The results revealed that the inclusion of lime, CCR, and PWG significantly improved the index and strength properties of the soil. A progressive increase in liquid limit, plastic limit and a reduction in plastic index for mixes L6 and L6-C2-P1 recording 10.91% and 23.47% respectively below that of the natural soil (25.32%) was observed with increasing stabilizer content, indicating enhanced volumetric stability and reduced susceptibility to shrink–swell behavior. The strength characteristics of the stabilized soil showed slight improvement. UCS and CBR values increased considerably with stabilization, demonstrating enhanced load-bearing capacity and resistance to deformation. These improvements are attributed to pozzolanic reactions between lime and CCR, which produced cementitious compounds that bonded soil particles together, as well as the reinforcing and pore-filling effects of PWG. However, beyond certain stabilizer proportions, a slight reduction in strength was observed, suggesting the presence of an optimum mix content. Among the blends investigated, L6–C1–P0.5 (6% Lime-1% Calcium carbide residue-0.5% Plastic waste granules) and L6–C2–P0.5 (6% Lime-2% Calcium carbide residue-0.5% Plastic waste granules) exhibited the best overall performance in terms of reduced plasticity, increased strength, and improved bearing capacity. The findings of this study confirm that the combined use of lime, CCR, and PWG is an effective and sustainable method for improving the geotechnical behavior of clayey soils. The stabilized soil showed improvement in index and strength properties making it suitable for use in road construction and foundation support. Furthermore, the utilization of industrial and plastic waste materials contributes to environmental sustainability by reducing waste disposal problems and minimizing dependence on conventional stabilizers. This study therefore provides a practical and eco-friendly solution for soil stabilization, particularly in developing regions where such waste materials are readily available.

# TABLE OF CONTENTS

Title Page .........................................................................................................................................i
Declaration ......................................................................................................................................ii
Certification ...................................................................................................................................iii
Dedication ......................................................................................................................................iv
Acknowledgements .........................................................................................................................v
Abstract ..........................................................................................................................................vi

## Chapter One: Introduction ..............................................................................................................1

1.1 Background of the Study ..........................................................................................................1
1.2 Statement of the Problem ..........................................................................................................3
1.3 Aim of the Study .......................................................................................................................3
1.4 Scope of the Study ....................................................................................................................3
1.5 Significance of Study ................................................................................................................3

## Chapter Two: Literature Review ....................................................................................................5

2.1 Introduction ...............................................................................................................................5
2.2 Soil as an Engineering Material ................................................................................................6
2.2.1 Nature and Classification of Soils ..........................................................................................6
2.2.2 Types of soil and their engineering significance....................................................................7	         2.2.3 Engineering Properties of Clay Soils………………………………………………………..7        2.2.4 Dealing with problematic soils……………………………………………………………...7       2.2.5 Introduction to soil stabilization…………………………………………………………….8

2.3 Soil Stabilization ......................................................................................................................8
    2.3.1 Concept of Soil Stabilization .............................................................................................8
    2.3.2 Importance of Soil Stabilization ........................................................................................9
    2.3.3 Methods of Soil Stabilization ...........................................................................................10
    2.3.4 Waste-Based stabilizer as alternative stabilization techniques ........................................11

2.4 Mechanism, prospects and limitation of conventional stabilizers (Lime & Cement)..............13
    2.4.1 Overview of Conventional Stabilizers .............................................................................13
    2.4.2 Mechanism of Lime Stabilization ....................................................................................13
    2.4.3 Mechanism of Cement Stabilization ................................................................................14
    2.4.4 Prospect of Lime and cement stablization........................................................................14
    2.4.5 Limitations of lime and cement stabilization....................................................................15
    2.4.6 Motivation for Alternatives ..............................................................................................16

2.5 Trends, Mechanism and Gaps of Waste-based soil stabilization techniques………...............17       2.5.1 Overview of waste based stabilization……………………………………………………..17       2.5.2 Common waste material used in soil stabilization…………………………………………17       2.5.3 Mechanisms of waste based stabilization………………………………………………….19       2.5.4 Prospect of waste based stabilization………………………………………………….…...19        2.5.5 Limitations and challenges of waste based stablizers……………………………………...20       2.5.6 Research gaps and the rationale of ternary blending………………………………………20

2.6 Review of stand-alone or binary combination of CCR and PWG or with other admixtures...21
    2.6.1 Calcium Carbide Residue (CCR) .....................................................................................21
    2.6.2 Plastic Waste Granules (PWG) ........................................................................................22

2.7 Previous research on the use of CCR and PWG as stand-alone or binary or ternary combination with other stabilizers……………………………………………………………...................................23	      2.7.1 Synergistic potential of CCR and PWG in ternary blend………………………………….24	       2.7.2 Basis for mix design and experimental framework………………………………………..24

2.8 Present status of research on ternary combination of lime, CCR and PWG………...............25

## CHAPTER THREE: MATERIALS AND METHODS ...............................................................27

3.1 Sampling of Materials .............................................................................................................27
    3.1.1 Clay Soil ..........................................................................................................................27
    3.1.2 Lime .................................................................................................................................27
    3.1.3 Calcium Carbide Residue ................................................................................................27
    3.1.4 Plastic Waste Granules ....................................................................................................27

3.2 Experimental Programme .......................................................................................................27
3.2.1 Natural Clay Soil ..................................................................................................................28       3.2.2 Stabilized soil ……………………………………………………………………………...28       3.2.3 Sample preparation.…………………………………………………………………….….28

3.3 Laboratory Tests and Procedures ............................................................................................29
3.3.1 Specific Gravity……………………………………………………………………………29
3.3.2 Grain size distribution ……………………….....................................................................30        3.3.3 Atterberg limit …..……………...…………………………………………………………32        3.3.4 Standard compaction test……..............................................................................................34                      3.3.5 California bearing ratio test(CBR) test ................................................................................35
3.3.6 Unconfined compression strength test .................................................................................36

CHAPTER FOUR: RESULTS AND DISCUSSION ...................................................................38
4.1 Engineering properties of natural soil......................................................................................38	          4.2 Effect of consistency limits of stabilized soil..........................................................................40
4.3 Effect of lime–CCR–plastic waste, on the compaction characteristics of the stabilized soil..41
4.4 Effect of lime CCR and plastic waste, on the strength of the stabilized soil...........................42
4.5 Effect of lime CCR and plastic waste on California Bearing Ratio (CBR) of the Stabilized Soil……………………………………………………………………………………………….43

## CHAPTER FIVE: CONCLUSION AND RECOMMENDATIONS ...........................................45		 5.1 Conclusion………………………………………………………………………………...…45      	 5.2 Recommendation…………………………………………………………………………….45

## REFERENCES ........................................................................................................................47-56

## APPENDIX………………………………………………………………………………....57-10

LIST OF TABLES												Table 2.1: summary of key studies....……...……………………………………….…….21		Table 3.1: Mixture and their Acronyms………………………………………………….29	 	Table 4.1: Physical and chemical properties of the soil………………………………….39

LIST OF FIGURES

Fig 4.1: Particle size distribution curve of natural soil sample……………………………..40

Fig 4.2: consistency limit of Stabilized Soil…………………………………..….……..........41

Fig 4.3: compaction chart for Lime-Calcium Carbide Residue-Plastic Waste Granules …...42

Fig 4.4: UCS chart for Lime-CalciumCarbideResidue-PlasticWasteGranules ……….……...43

Fig 4.5: CBR chart for Lime-CCR-PWG…………………………………………………….44

CHAPTER ONE

INTRODUCTION

1.1 Background of the Study

Soil is a loose, unconsolidated inorganic material covering the Earth's crust, formed through mechanical and chemical weathering of solid rocks (Maneeth et al., 2014). Natural soils exhibit variations in their properties and are predominantly heterogeneous. Soils display considerable diversity in structure, texture, and composition across different formation settings, which affects their physical, engineering and geotechnical properties. Following initial formation, soils experience ongoing and continuous alterations from external stresses, chemical reactions, and weathering (Craig, 2004). The intrinsic characteristics of certain soil types restrict their use in specific engineering projects, necessitating modifications to these properties to suit particular engineering requirements.

Clay are widely distributed in Nigeria but pose significant challenges for geotechnical engineers in construction applications (Gbadamosi, 2021). They are unsuitable due to low strength and high susceptibility to volume changes upon moisture exposure. The challenge of instability of clay is as a result of swelling nature of expansive clay material thereby making the soil unsuitable material for construction in foundation of buildings, highway, railway or any other engineering structures (Ogunribido and Abiola, 2015).

When unsuitable soils like clay are encountered on-site, engineers first consider alternatives such as removal and replacement, bypassing the area, surcharging, groundwater control, or deep foundations. If these options are impractical or uneconomical, stabilization is adopted to improve the soil’s engineering properties, as it has proven to be the most effective and economical approach for enhancing soil properties (Behnood, 2018). Numerous studies have investigated various stabilization techniques, such as lime, cement, and agricultural waste ashes, to enhance the performance of clay for construction purposes (Al-Mukhtar et al. 2014).

Soil stabilization involves the use of stabilizing agents (binder materials) in weak soils to improve its strength and other properties. Cementation is the main aim of the process referred to as ‘soil stabilization’ used in practical geotechnical applications to improve the properties of the soil in terms of strength, stiffness and hydraulic behavior which is why chemical stabilization agents: Portland cement, lime, asphalt, biomass ashes, calcium chloride are sodium chloride are used. Soil conditions, stabilizer properties, and construction types (roads and houses) decide the adequacy of these added substances (Etekume and Onwualu, 2020). The conventional stabilizing agent for chemical stabilization are cements and lime but with the constant rise in the cost of this additives which is influencing the total construction cost coupled with the environmental impact of their production as it is known to be energy intensive and also emits CO₂, which affects the atmosphere negatively.

Lime stabilization is a prevalent technique for strengthening weak fine-grained soils across various regions. It involves mixing quicklime or hydrated lime into the soil, where chemical reactions bind particles, improving strength and workability. However, lime has limitations, including delayed strength gain due to carbonation, swelling from sulfates, and degradation of organic matter, which can affect soil ecology. Environmentally, lime production emits significant CO₂, generates dust from mining, and risks water contamination. In bid to curb this due to the cost and environmental impact alternatives are sorted for to eradicate or reduce the use of these stabilizing agents.

According to Geyer et al. (2017), there is growing international concern over the escalation of plastic waste, which is increasingly posing a severe nuisance to the environment through persistent pollution of terrestrial, aquatic, and marine ecosystems. Despite various measures implemented to curb plastic production and disposal such as recycling mandates, bans on single-use items, and waste management policies these efforts have largely proven ineffective or yielded low results, with global plastic production continuing to surge and over 79% of accumulated waste ending up in landfills or the natural environment (Geyer et al., 2017). The gap between growing plastic waste and poor solutions has led to new ways of reusing it like it incorporation into soil stabilization, especially in places like Nigeria where both waste and weak soil are big problems.

Calcium carbide residue (CCR) is a by-product of acetylene gas manufactured from calcium carbide and is mainly calcium hydroxide. There has been interest in its utilization as a complementary ingredient for soil stabilization because of its ability to catalyze cementation in clay soil. Global Calcium Carbide Residue (CCR) production is approximately 28–32 million metric tons annually, with 55–60% (~15–19 million metric tons) disposed of in landfills or ponds (Bawab et al., 2025). The calcium carbide residue can improve strength and resistance to moisture. On the other hand, this industrial waste can alleviate disposal concerns while reducing environmental ramifications posed by lime.

1.2 Statement of Problem

Clay in its natural state is highly problematic when used as a supporting soil in construction due to its high plasticity, low shear strength and sensitivity to moisture variations which leads to swelling and shrinkage and reduced load bearing capacity. The challenge of plastic pollution which is of growing concern too and the increasing cost of lime despite its high energy intensive production coupled with it environmental impact because of CO2 emission as stabilizing agent with calcium carbide residue a waste product of acetylene gas in manufacturing industry and it also polluting the environment and is also readily available have necessitate the search for cheaper and locally available alternatives. Hence, this project involves a study on the possible use of a ternary blend of lime, plastic waste granules and calcium carbide residue for stabilization of deficient soils.

1.3 Aim and Objectives

This study evaluates the effect of calcium-carbide residue and plastic waste granules in lime based clay subgrade, aiming to enhance strength, reduce lime use, lower carbon emissions and minimize environmental impact.

Objectives of the study are to:

- assess the index properties of the natural soil sample

- examine the engineering properties of the soil sample

- evaluate the engineering properties of the stabilized soil

1.4 Scope of the Study

This research focuses on evaluating the geotechnical enhancement of clayey soil, a predominant deposit in Ado-Ekiti, Nigeria, stabilized with a ternary mix of lime, calcium carbide residue (CCR), and plastic waste granules. The study is strictly laboratory-based, assessing chemical properties through targeted geotechnical tests, including unconfined compressive strength (Kamei et al., 2013).

Lime promotes pozzolanic reactions, reduces plasticity, and improves shear strength in fine-grained soils. CCR, rich in calcium oxide, provides cementitious properties similar to lime.

1.5 Significance of the Study

This study provides a sustainable, cost-effective method to stabilize clayey soil using lime, CCR, and plastic waste, improving it geotechnical properties for construction while reducing waste, carbon emissions, and costs. It supports green infrastructure, informs policy, and promotes circular economy practices in Nigeria.

CHAPTER TWO

LITERATURE REVIEW

2.1 Introduction

Soil is one of the most important materials in civil engineering because it forms the natural foundation for most structures such as buildings, roads, bridges, and embankments. The safety, stability, and performance of these structures depend largely on the properties of the soil supporting them. However, natural soils often vary widely in their engineering behavior due to differences in composition, texture, and origin. In many parts of Nigeria and other tropical regions, soils exhibit poor engineering characteristics, particularly clay soils, which tend to have low strength and excessive volume changes with variations in moisture content (Onyelowe et al., 2020).

When engineers encounter problematic soils on site, several approaches can be considered. One option is to bypass the weak area by rerouting the structure. Another is to replace the poor soil with better-quality material obtained elsewhere. In some cases, bridging methods such as using piles, rafts, or reinforced foundations are adopted to transfer structural loads to deeper, more competent layers. However, these methods are usually expensive and not always feasible in large-scale or low-cost projects. The most practical and economical approach to improving weak soils is stabilization, which modifies the existing soil to enhance its engineering performance (Osinubi et al., 2019).

Soil stabilization has therefore become an essential part of geotechnical engineering practice. Traditionally, materials such as lime and cement have been widely used to improve the strength and stability of problematic soils. Yet, the production of these materials is energy-intensive and releases large amounts of carbon dioxide (CO₂), contributing significantly to environmental pollution. According to Ige et al., 2024, the cement industry alone accounts for approximately eight percent of global CO₂ emissions, while lime production is also a major contributor. These environmental challenges have motivated researchers to explore more sustainable alternatives, particularly waste-based materials that can both improve soil properties and reduce pollution (Akeem et al., 2023).

In Nigeria, clay soils are among the most widespread soil types, especially in the southern and central regions. They are often encountered during construction and are known for their poor load-bearing capacity, high plasticity, and potential for swelling and shrinkage. Because of their abundance, it is more practical to improve them through stabilization than to completely replace them. Thus, this study focuses on clay as a foundation soil that can be enhanced using ternary blended mixtures of Lime, Calcium Carbide Residue (CCR) and Plastic Waste Granules (PWG) two waste materials with great potential for sustainable soil improvement.

This chapter therefore reviews relevant literature on the nature and classification of soils, the engineering behavior of clay, and various soil stabilization methods. Special attention is given to waste-based stabilizers such as CCR and PWG, including their individual and combined effects on soil properties, previous research findings, and identified gaps that justify the present study.

2.2 Soil as an Engineering Material

2.2.1 Nature and Classification of Soils

Soil is a naturally occurring material composed of mineral particles, organic matter, water, and air. It forms through the weathering of rocks and the decomposition of organic materials over time. The engineering behavior of a soil depends on its particle size, composition, structure, and environmental conditions. For geotechnical purposes, soils are commonly classified into coarse-grained soils (such as gravels and sands) and fine-grained soils (such as silts and clays) based on particle size distribution (Das & Sobhan, 2017).

The Unified Soil Classification System (USCS) and the AASHTO system are the most widely used methods of soil classification. The USCS categorizes soils according to grain size and plasticity, while AASHTO focuses on their suitability for construction purposes. Coarse-grained soils such as gravels and sands generally have good drainage, high bearing capacity, and low compressibility, making them suitable for most engineering applications. Fine-grained soils, on the other hand, retain water, have low permeability, and often exhibit plastic and compressible behavior, which can be problematic for foundations (Craig, 2012).

2.2.2 Types of Soils and Their Engineering Significance

Different soil types behave differently under load. Gravelly soils provide excellent support and are ideal for heavy foundations due to their high shear strength and minimal settlement. Sandy soils offer good bearing capacity but may suffer from liquefaction under dynamic loading. Silty soils are more compressible and tend to lose strength when saturated. Clay soils, however, present the greatest challenge due to their expansive nature, low shear strength, and high plasticity (Mitchell & Soga, 2005).

Owing to these properties, clay is often referred to as a problematic soil in foundation engineering. In Nigeria, large expanses of land are covered with clayey deposits, especially in areas such as Ekiti, Enugu, Anambra, Benue, and parts of the northern states (Dansarai et al. (2020). Replacing or bypassing these soils during construction is usually uneconomical, making stabilization a more practical and cost-effective option.

2.2.3 Engineering Properties of Clay Soils

Clay soils are fine-grained and have a large specific surface area, which makes them sensitive to water. They exhibit high plasticity, low permeability, and low bearing strength, making them unsuitable for direct foundation support without treatment (Osinubi et al., 2019). When wet, clay expands and loses strength, leading to settlement or structural instability. During dry periods, it shrinks, causing cracks in both the soil and structures founded upon it. These repeated cycles of swelling and shrinkage can lead to foundation distress and wall cracking in buildings.

The behavior of clay depends largely on the type of clay mineral present. Montmorillonitic clays expand and contract significantly with moisture changes, while kaolinitic clays are relatively stable. Poor drainage further aggravates these problems by keeping the soil in a saturated state for prolonged periods (Mitchell & Soga, 2005).

2.2.4 Dealing with Problematic Soils

When problematic soils such as clay are encountered on site, engineers have several options. The most direct method is to remove and replace the weak soil with more competent material. Alternatively, structures may be bridged over weak zones using deep foundations like piles or raft systems that transfer loads to deeper, stronger layers. In some cases, the project alignment may be bypassed to avoid weak soils altogether. However, these solutions are often expensive and time-consuming (Ola, 1974).

As a result, soil stabilization has become the most commonly adopted and economical approach to improving weak soils, especially when large areas are involved. Stabilization techniques modify the existing soil to improve its strength, reduce compressibility, and control its volume change characteristics.

2.2.5 Introduction to Soil Stabilization

Soil stabilization refers to any process that improves the physical and mechanical properties of soil to make it suitable for construction. It can be achieved through various techniques, generally classified as mechanical, chemical, or biological methods (Craig, 2012). Mechanical stabilization involves mixing soils of different types or compacting the soil to achieve higher density. Chemical stabilization, on the other hand, introduces additives such as lime, cement, or waste-based binders to enhance the soil’s strength and durability. Biological methods, though less common, involve the use of microorganisms to improve soil structure.

Among these techniques, chemical stabilization has gained the most attention because it effectively improves the strength, bearing capacity, and durability of fine-grained soils such as clay. However, with increasing environmental awareness, recent research has focused on using waste-derived additives like Calcium Carbide Residue (CCR), Plastic Waste Granules (PWG), Rice Husk, Sawdust, Sugarcane Bagasse etc. as sustainable alternatives to conventional chemical stabilizers.

## 2.3 Soil Stabilization

### 2.3.1 Concept of Soil Stabilization

Soil stabilization is the process of improving the engineering properties of soil to make it suitable for supporting structures such as buildings, roads, and embankments. The main aim is to enhance strength, stiffness, and load-bearing capacity while reducing plasticity, compressibility, and susceptibility to moisture variation (Craig, 2012). In practice, stabilization transforms a weak or problematic soil into a reliable foundation material that can withstand imposed structural loads.

In many parts of the world, and particularly in Nigeria, the natural soils encountered on construction sites often fail to meet the required engineering standards. This is especially true for fine-grained soils such as clays, which are known for their high plasticity and tendency to shrink and swell with changing moisture conditions (Osinubi et al., 2019). These variations in volume can cause severe damage to structures, including foundation cracking, wall deformation, and in extreme cases, structural failure.

Stabilization has become a critical process in geotechnical engineering practice. It allows engineers to modify and improve the behavior of in-situ soils through mechanical or chemical means, thereby ensuring the long-term stability and safety of constructed facilities.

### 2.3.2 Importance of Soil Stabilization

The importance of soil stabilization lies in its ability to enhance the performance of weak soils that would otherwise be unsuitable for construction. For any structure, the foundation is only as stable as the soil beneath it. If the subgrade or subsoil lacks sufficient bearing capacity, the result can be differential settlement or total failure of the structure. Stabilization techniques help prevent these problems by improving soil strength and stiffness while reducing compressibility and water sensitivity (Das & Sobhan, 2017).

In Nigeria, where expansive clay soils are common, the need for stabilization is even greater. These soils absorb large amounts of water during the rainy season and lose it during dry periods, causing cycles of expansion and contraction. Such movements lead to cracks in walls, floors, and pavements, particularly in lightly loaded buildings and road structures (Onyelowe & Van, 2020).

In addition to technical performance, stabilization provides economic and environmental benefits. Instead of removing and replacing poor soils a costly and time-consuming process engineers can improve the soil in place using locally available materials. This reduces both the cost and environmental impact associated with transportation and quarrying.

### 2.3.3 Methods of Soil Stabilization

Soil stabilization techniques are broadly grouped into three main categories: mechanical, chemical, and biological methods (Mitchell & Soga, 2005).

A. Mechanical Stabilization: Mechanical stabilization involves physical modification of the soil to improve its properties. This can include compaction, blending of different soil types to achieve better gradation, or adding reinforcement materials such as geotextiles and fibers. Although effective for granular soils, this method often provides limited improvement for clayey soils because their strength and deformation behavior are governed more by chemical and mineralogical interactions than by physical rearrangement.

B. Chemical Stabilization: Chemical stabilization involves the addition of stabilizing agents that react chemically with the soil to improve its engineering characteristics. Traditional stabilizers such as lime and cement have been widely used for this purpose. They react with clay minerals and soil moisture to form cementitious compounds that increase strength and durability. The process typically involves ion exchange, flocculation, and pozzolanic reactions, which bind soil particles into a stable mass (Das & Sobhan, 2017). Among the available methods, chemical stabilization remains the most effective for the fine-grained soils, particularly clay. When chemical stabilizers such as lime or cement are added to clayey soils, they undergo a series of reactions that alter soil structure and improve its mechanical properties.

Lime, for example, provides calcium ions that replace sodium and hydrogen ions in the clay structure, leading to flocculation and agglomeration of clay particles. This reduces plasticity and improves workability. Over time, pozzolanic reactions occur between lime and the silica or alumina in the soil, producing calcium silicate hydrate (C–S–H) and calcium aluminate hydrate (C–A–H) compounds that impart long-term strength and stability (Mitchell & Soga, 2005).

Similarly, cement stabilization relies on hydration reactions to form cementitious compounds that bind soil particles together, creating a dense and durable matrix. The result is a significant improvement in bearing capacity and resistance to water-related deterioration.

However, despite their effectiveness, the use of lime and cement is increasingly being questioned due to their economic and environmental drawbacks. The production of these materials is energy-intensive and contributes significantly to greenhouse gas emissions, particularly CO₂ (Obinna et al., 2022). Additionally, in developing countries like Nigeria, the high cost of lime and cement poses a serious challenge, as these materials are often imported or produced at considerable expense. This increases overall construction costs, making large-scale stabilization projects less affordable.

These concerns rising costs, high energy consumption, and environmental impact have driven researchers toward identifying cheaper, locally available, and eco-friendly alternatives such as industrial and agricultural wastes.

C. Biological Stabilization: Biological stabilization is a relatively new and environmentally friendly approach that uses microbial activity to improve soil strength. Microorganisms can precipitate calcium carbonate in the soil, effectively binding particles together. Although this technique has shown promise in laboratory studies, it is still at a developmental stage and has not yet been widely adopted in construction practice (Akeem et al., 2023).

Among the available methods, chemical stabilization remains the most effective for fine-grained soils, particularly clays. When chemical stabilizers such as lime or cement are added to clayey soils, they undergo a series of reactions that alter the soil’s structure and improve its mechanical properties.

### 2.3.4 Waste-Based Stabilizer as Alternative Stabilization Technique

The global shift toward sustainable construction has encouraged the use of waste-derived materials in soil stabilization. Industrial by-products such as fly ash, rice husk ash, ground granulated blast furnace slag (GGBS), and calcium carbide residue (CCR) have demonstrated significant potential due to their pozzolanic properties (Onyelowe et al., 2019). These materials are not only cheaper but also reduce environmental pollution by diverting waste from landfills.

Calcium Carbide Residue (CCR) is a waste material generated during the production of acetylene gas, around 4.3 billion tons of Calcium Carbide Residue are generated annually worldwide (Mahmmod & Abbas, 2025). Chemically, it consists largely of calcium hydroxide, which gives it similar reactivity to hydrated lime.

Its use in soil stabilization has been shown to reduce plasticity, enhance compressive strength, and improve the bearing capacity of clayey soils (Almuaythir et al., 2024). Importantly, because CCR is often available as an industrial waste in Nigeria, it provides a low-cost alternative to lime for large-scale stabilization projects.

Plastic Waste Granules (PWG), obtained from recycled plastic materials, contribute to stabilization in a different way. Instead of reacting chemically, PWG improves the physical behavior of soils by reinforcing the soil structure, enhancing inter-particle bonding, and reducing brittleness. The inclusion of plastic granules increases ductility and tensile strength, making the soil more resistant to cracking and deformation under load (Akeem et al., 2023).

Beyond CCR and PWG, a wide range of waste-derived materials has been explored in recent research as sustainable alternatives for improving problematic soils. For example, rice husk ash (RHA), a by-product from rice milling, is rich in silica and has been shown to reduce plasticity and improve strength when incorporated into clayey soils, either alone or with traditional binders like lime or cement, making it a promising stabilizer for expansive soils (Blayi, Kakrasul, & Hamad, 2025). Similarly, agricultural residues such as bagasse ash, produced from sugarcane processing, have demonstrated the ability to enhance compressive strength and reduce swell potential of treated soils when used as partial replacements for cementitious stabilizers (Awadalseed, Zhao, Sun, Huang, & Liu, 2023). Industrial by-products such as steel slag and iron tailing powder have also been evaluated and found to significantly increase mechanical strength when combined with cement in stabilized soil mixtures, highlighting the potential of mineral waste materials to improve engineering performance (Cai et al., 2025). Comprehensive reviews further confirm that waste materials like fly ash, rice husk ash, and other agricultural or industrial by-products can meet engineering objectives while promoting environmental sustainability and resource efficiency in soil stabilization practices (Shinde, Sangale, Pranita, Sanagle, & Roham, 2024)

When used together in a ternary blend, Lime, CCR and PWG complement each other’s properties CCR provides the chemical stabilization needed for strength, while PWG enhances the soil’s structural flexibility and toughness. This combined approach has shown promise in improving the performance of clay subgrades used in both road and building foundation applications.

The application of waste materials such as CCR and PWG for soil stabilization offers numerous benefits; reduction of CO₂ emissions and the recycling of waste materials also cost reduction by utilizing inexpensive locally available materials, there is improved waste management by reducing the accumulation of industrial and plastic wastes, enhanced performance through improved strength, durability, and resistance to moisture and promotion of sustainable construction practices as well as support for circular economy principles.

In Nigeria, where clay soils are abundant and both CCR and plastic wastes are readily available, the adoption of waste-based stabilization is a practical and sustainable approach. It addresses multiple challenges simultaneously poor soil performance, high construction costs, and environmental degradation.

## 2.4 Mechanism, Prospects and Limitations of Conventional Stabilizers (Lime & Cement)

### 2.4.1 Overview of Conventional Stabilizers

Lime and cement are the conventional stabilizers and they are the most widely used chemical stabilizers in geotechnical engineering. They have been applied for several decades to improve the engineering performance of weak soils, particularly fine-grained soils such as clays and silty clays. Their effectiveness lies in their ability to chemically react with soil minerals and water to form stable compounds that enhance strength, stiffness, and durability (Mitchell & Soga, 2005).

Lime stabilization is commonly adopted for expansive and highly plastic clays, while cement is often used for granular or silty soils. However, both have been found effective for improving a wide range of problematic soils when applied in appropriate proportions and under suitable curing conditions (Das & Sobhan, 2017).

In Nigeria, lime and cement stabilization are well-established techniques used to improve foundation soils for both road and building construction. However, the rising cost of these materials and growing environmental concerns have encouraged researchers to explore alternative stabilizers derived from waste materials.

### 2.4.2 Mechanism of Lime Stabilization

Lime stabilization works primarily through three mechanisms namely cation exchange, flocculation-agglomeration, and pozzolanic reaction. When lime (CaO or Ca(OH)₂) is added to clay soil, it dissociates in water to release calcium ions (Ca²⁺) and hydroxyl ions (OH⁻). The calcium ions replace sodium and hydrogen ions adsorbed on the surface of clay minerals. This cation exchange causes the fine clay particles to flocculate and form larger aggregates, reducing plasticity and improving workability (Little, 1995).

Pozzolanic reactions occur between the calcium from lime, the silica and alumina naturally present in the clay which is time dependent. These reactions produce cementitious compounds calcium silicate hydrate (C–S–H) and calcium aluminate hydrate (C–A–H) which bind the soil particles together, significantly increasing strength and stiffness (Akula & Little, 2020).

The effectiveness of lime stabilization depends on several factors such as lime content, soil mineralogy, curing period, and temperature. Generally, the longer the curing period, the higher the strength gain due to continued pozzolanic activity (Ahmadullah & Chrysochoou, 2024).

### 2.4.3 Mechanism of Cement Stabilization

Cement stabilization involves the hydration of cement in the presence of soil and water, producing binding compounds that strengthen the soil matrix. When cement is mixed with soil, hydration reactions lead to the formation of calcium silicate hydrate (C–S–H) and calcium aluminate hydrate (C–A–H) the same compounds responsible for the hardening of concrete (Dash & Hussain, 2012).

These compounds coat and bind soil particles together, reducing voids, permeability, and compressibility while increasing load-bearing capacity. Unlike lime, which mainly reacts with clay minerals, cement can stabilize a broader range of soils, including granular and silty materials (Komolafe & Osinubi, 2019).

Cement stabilization is particularly effective in improving the immediate strength of soil due to its rapid hydration reactions. However, its efficiency in highly plastic clays is sometimes limited because of difficulty in achieving uniform mixing and the potential for shrinkage cracking during drying.

### 2.4.4 Prospect of Lime and Cement Stabilization

The success of lime and cement stabilization in civil engineering applications is well documented. Numerous studies have demonstrated significant improvements in soil strength, workability, and durability.

In Nigeria and other developing countries, both lime and cement have been widely used to stabilize clay subgrades for road pavements and building foundations (Onyelowe et al., 2020). These stabilizers improve the unconfined compressive strength (UCS), California Bearing Ratio (CBR), and shear strength of soils, making them suitable for load-bearing applications.

Lime stabilization has also proven effective in reducing swelling and shrinkage behavior in expansive clays, a critical concern for foundation design in tropical regions. Similarly, cement-stabilized soils exhibit increased resistance to erosion, moisture ingress, and deformation under load, ensuring long-term performance.

Beyond mechanical improvements, the use of lime and cement contributes to the overall sustainability of construction by enabling the reuse of in-situ soils rather than requiring costly excavation and replacement. This has made chemical stabilization a preferred solution in areas where weak or problematic soils are encountered.

### 2.4.5 Limitations of Lime and Cement Stabilization

Despite their effectiveness, lime and cement stabilization present several limitations that restrict their long-term sustainability and economic viability, particularly in developing nations.

A. Environmental Impact: The production of lime and cement is energy-intensive and contributes significantly to greenhouse gas emissions. The calcination of limestone, a key process in lime and cement manufacture, releases large quantities of CO₂ into the atmosphere (Hilaloglu, Kanwal, Almarshoud, & Al-Ghamdi, 2026). This makes them major contributors to global warming and environmental degradation.

B. High Energy Consumption: The manufacturing process involves quarrying, heating, and grinding, all of which require substantial energy. According to global estimates, cement production accounts for about 8% of total anthropogenic CO₂ emissions, while lime production contributes about 1% (Neale et al., 2021). These figures have raised concerns about the environmental sustainability of traditional soil stabilization methods.

C. Economic Constraints: In Nigeria, the high cost of purchasing lime and cement has become a major challenge for both public and private construction projects. The prices of these stabilizers have increased steadily due to rising energy costs, currency fluctuations, and transportation expenses. Consequently, their use in large-scale soil improvement works often escalates overall construction costs, making projects less affordable for low-income communities (Nnadi & Najjobyo, 2025).

D. Material Availability and Transportation: In remote or rural areas, lime and cement may not be readily available. The need to transport these materials over long distances adds to project costs and delays. In contrast, locally available waste materials such as calcium carbide residue, plastic waste, rice husk, fly ash, sugarcane bagasse among others can be obtained at little or no cost, offering an attractive alternative.

E. Durability Concerns: Although lime and cement stabilization improve short- and medium-term strength, their long-term performance can be affected by environmental factors such as leaching, cyclic wetting and drying, or sulfate attack. Over time, these conditions can degrade the cementitious bonds formed in stabilized soils, leading to strength loss or cracking (Dash & Hussain, 2012).

### 2.4.6 Motivation for Alternatives

Considering these limitations, there is a growing interest in identifying sustainable, low-cost, and eco-friendly alternatives to lime and cement. Waste-based stabilizers such as calcium carbide residue (CCR), rice husk ash, fly ash, and plastic waste granules (PWG) among others are gaining attention for their ability to partially or wholly replace conventional stabilizers.

These alternatives not only reduce the environmental footprint associated with lime and cement production but also help manage waste materials that would otherwise contribute to pollution. Moreover, the utilization of such wastes aligns with global sustainable development goals (SDGs), particularly those related to responsible consumption, climate action, and sustainable infrastructure (Akeem et al., 2023).

The present research therefore seeks to investigate the geotechnical performance of clay soils stabilized with a ternary blend involving CCR, PWG, and lime, as a step toward developing more sustainable soil improvement strategies.

2.5 Trends, Mechanisms and Gaps of Waste-based Soil Stabilization Technique

2.5.1 Overview of Waste-Based Stabilization

In recent decades, the search for sustainable construction practices has led to a growing interest in using industrial and agricultural waste materials for soil stabilization. The motivation for this trend is two fold: the need to mitigate the environmental effects of conventional stabilizers such as lime and cement, and the desire to recycle waste materials that pose disposal challenges (Shinde et al., 2024).

Waste-based stabilization offers a dual advantage. It improves the engineering properties of problematic soils while reducing environmental pollution and the carbon footprint associated with traditional binders. Additionally, in developing countries like Nigeria where the high cost of cement and lime can significantly raise construction expenses waste-derived stabilizers provide a more economical and sustainable option (Akeem et al., 2023).

These materials often contain reactive silica, alumina, or calcium compounds that can undergo pozzolanic reactions similar to those seen in lime or cement stabilization. Common examples include fly ash, rice husk ash (RHA), ground granulated blast furnace slag (GGBS), cement kiln dust (CKD), calcium carbide residue (CCR), and plastic waste. Each of these wastes has been studied for its potential to improve soil strength, durability, and volume stability.

    - Common Waste Materials Used in Soil Stabilization

A. Fly Ash: Fly ash is a by-product of coal combustion in thermal power plants. It contains significant amounts of silica and alumina, which make it pozzolanic in nature. When mixed with lime or cement, fly ash enhances the formation of cementitious compounds, improving soil strength and durability (Alqawasmeh, 2025). Studies have shown that fly ash can effectively reduce the plasticity and increase the bearing capacity of clayey soils. However, its reactivity alone is often insufficient for high-strength applications, necessitating the addition of a small quantity of lime or cement.

B. Rice Husk Ash (RHA): RHA is produced from the controlled burning of rice husks, a common agricultural waste in Nigeria and other rice-producing countries. It is rich in amorphous silica, which reacts with calcium hydroxide to form cementitious products. The use of RHA in stabilization improves soil strength and reduces plasticity, while also addressing the environmental problem of open-field burning of rice husks (Ettu et al., 2013).

C. Ground Granulated Blast Furnace Slag (GGBS): GGBS, a by-product of the steel industry, has latent hydraulic properties that can be activated by lime or alkalis. Its inclusion in soil stabilization has been found to enhance the compressive strength and reduce the permeability of treated soils (Amadi et al., 2019). However, GGBS is not readily available in all regions of Nigeria, which may limit its widespread use.

D. Cement Kiln Dust (CKD): CKD is a fine-grained material collected from the exhaust gases during cement production. It contains unreacted lime and other oxides, giving it a high pH and chemical reactivity. CKD can partially replace cement or lime in soil stabilization, although the variability of its composition can lead to inconsistent results (Al-Bakri, Ahmed, & Hefni, 2022).

E. Calcium Carbide Residue (CCR): CCR is a waste by-product from the generation of acetylene gas. Chemically, it is primarily composed of calcium hydroxide, similar to hydrated lime, and hence exhibits comparable pozzolanic reactivity. Studies have demonstrated that CCR can effectively improve the strength and reduce the plasticity of clayey soils (Anjum et al., 2025). It is produced locally in Nigeria from welding and gas plants, it presents a cost-effective and sustainable alternative to lime for large-scale soil stabilization.

F. Plastic Waste Granules (PWG): Plastic waste poses a major global environmental challenge due to its non-biodegradability. Plastic pollution has emerged as one of the most pressing environmental issues of the 21st century. Globally, plastic production and disposal have risen dramatically since the mid-20th century, with hundreds of millions of tonnes of plastic waste generated annually and only a small fraction recycled, leading to pervasive contamination of terrestrial, freshwater, and marine environments. Plastic debris persists for centuries because of its non-biodegradable nature, disrupting ecosystems and posing risks to wildlife and human health (Felix & Raphael, 2025). Nigeria faces similarly severe challenges. As Africa’s most populous nation, plastic consumption and waste generation have increased rapidly, often outpacing waste management capacity. Studies estimate that plastic consumption in Nigeria doubles approximately every nine years, and the indiscriminate disposal of plastics especially sachet water bags and single-use packaging contributes to widespread terrestrial and aquatic pollution (Animashaun et al., 2025). The reuse of plastic waste in geotechnical engineering offers a practical method of reducing its environmental footprint. Plastic waste granules, fibers, or strips can improve soil performance through reinforcement rather than chemical reactions. They enhance ductility, reduce brittleness, and help in distributing stresses more evenly under load (Babu & Chouksey, 2011). Research has shown that the inclusion of waste plastics in clayey soils can significantly increase CBR values and improve the tensile and shear resistance of foundations and pavement layers (Hassan, Rasul, & Samin, 2021).

2.5.3 Mechanisms of Waste-Based Stabilization

The performance of waste-based stabilizers depends on the nature of the waste material and the type of soil being treated. Generally, the stabilization process involves one or more of the following mechanisms stated, these mechanisms collectively contribute to improved strength, durability, and load-bearing capacity of treated soils.

A.  Pozzolanic Reaction: Wastes containing reactive silica and alumina (such as CCR, fly ash, and RHA) react with calcium hydroxide to form cementitious compounds (C–S–H and C–A–H).

B.  Cation Exchange and Flocculation: Calcium-rich wastes such as CCR promote cation exchange in clays, leading to flocculation and reduced plasticity.

C. Physical Reinforcement: Non-reactive wastes like plastic granules act as discrete reinforcements within the soil, improving ductility and resistance to deformation.

D.  Void Filling: Fine-grained wastes help reduce soil porosity and permeability, resulting in a denser and more stable structure.

2.5.4 Prospect of Waste-Based Stabilization

Several researchers have reported significant success using waste-based stabilizers. Anjum et al. (2025) found that adding calcium carbide residue (CCR) to clayey and expansive soils can noticeably strengthen them. Soils treated with CCR tend to develop much higher unconfined compressive strength (UCS) and California Bearing Ratio (CBR) than untreated soils, making them more stable and better able to support structures. Luo et al. (2023) showed that mixing calcium carbide residue (CCR) with fly ash can noticeably improve the strength and overall performance of stabilized soils compared with untreated soils. Similarly, the inclusion of plastic waste in clayey soils has been shown to improve ductility and reduce cracking under cyclic loading, making it particularly beneficial for foundation soils subjected to repeated stresses (Babu & Chouksey, 2011). In addition, Akeem et al. (2023) noted that integrating industrial and agricultural wastes can provide comparable or even superior results to conventional stabilizers, while drastically cutting costs and emissions.

2.5.5 Limitations and Challenges of Waste-Based Stabilizers

Despite these promising results, several limitations hinder the full-scale adoption of waste-based stabilization. The chemical composition of waste materials can vary depending on their source and production process, which can lead to inconsistent results. Additionally, limited standardization means there are no universally accepted design standards or mix proportions for waste-based stabilizers, making field application challenging. Durability is also a concern, as some waste-based mixtures may show reduced long-term performance, particularly under aggressive environmental conditions. Finally, the lack of large-scale field trials means that most existing studies are laboratory-based, and reliable data on their real-world performance are still limited. Addressing these challenges requires systematic research, including experimental validation, standardization, and long-term performance monitoring.

2.5.6 Research Gaps and the Rationale for Ternary Blending

While several studies have investigated the use of individual waste materials such as CCR or plastic waste for soil stabilization, limited research has focused on their combined or ternary use with either lime or cement. Such ternary blends have the potential to harness the chemical reactivity of one and the mechanical benefits of another.

While there is still limited research specifically exploring the combined use of calcium carbide residue (CCR) and plastic waste granules for soil stabilization, studies on similar hybrid approaches suggest promising results. For example, incorporating CCR with reinforcing materials like polypropylene fibers has been shown to significantly improve soil strength and stability compared with using CCR alone (Luo et al., 2023). These findings highlight the potential benefits of investigating CCR–plastic waste combinations in future research.

Moreover, most past research has concentrated on road subgrades, with limited attention given to clay soils used in building foundations. This presents an important knowledge gap, especially in regions like Nigeria where clay soils are abundant and form the main bearing stratum for low- and medium-rise structures.

The present study therefore aims to fill this gap by evaluating the geotechnical performance of clay subgrade soils stabilized with a ternary blend of lime, calcium carbide residue (CCR) and plastic waste granules (PWG). The goal is to identify a cost-effective, environmentally sustainable, and technically reliable alternative to complete lime and cement for foundation stabilization.

Table 2.1: Summary of Key Studies

|  | Study | Soil Type | Mix Design | UCS (kPa) | CBR (%) | Swell (%) | Durability (Cycles) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1. | Singh, A., & Sugandhi, S. (2024). | Clay | 2% Lime or limestone & 0.4 plastic | — | 6.95 | 6.75% reduction | Not stated |
| 2. | Ojuri et al. (2022) | Silty clay | 6%Lime + 7 %Cow bone powder + 1.0 %Plastic waste | 201.7 | 61.7 (unsoaked) 37.6 (soaked) | — | 3days wet dry cycles |

2.6 Review of Stand-alone or Binary Combination of CCR and PWG or with other Admixtures

2.6.1 Calcium Carbide Residue (CCR)

Chemically, CCR exhibits behavior similar to hydrated lime because of its high calcium content and alkalinity. When introduced into clay soils, calcium ions from CCR replace weaker cations on the clay surface, leading to cation exchange and flocculation. This reduces plasticity, shrinkage, and swelling potential. Over time, the calcium hydroxide in CCR reacts with the silica and alumina in clay minerals to form cementitious products such as calcium silicate hydrate (C–S–H) and calcium aluminate hydrate (C–A–H), which contribute to the soil’s increased strength and stiffness (Onyelowe & Van, 2020).

The effectiveness of CCR depends on curing time, soil mineralogy, and dosage. Studies indicate that incorporating between 4% and 12% CCR can significantly enhance unconfined compressive strength (UCS) and California Bearing Ratio (CBR) values, while reducing swell potential (Horpibulsuk et al., 2013; Eberemu et al., 2018).

Beyond its technical merits, CCR offers both economic and environmental advantages. As an industrial by-product, it is readily available and inexpensive compared to lime. Utilizing CCR reduces waste disposal challenges, curtails CO₂ emissions associated with lime production, and supports sustainable construction practices. However, challenges such as inconsistent composition and limited standardization in field application remain issues that require further study.

2.6.2 Plastic Waste Granules (PWG)

Plastic waste granules (PWG) are processed fragments derived from recycled plastics such as polyethylene (PE), polypropylene (PP), and polyethylene terephthalate (PET). As global plastic consumption continues to rise, the accumulation of plastic waste has become a major environmental problem. Incorporating PWG into geotechnical engineering applications provides an avenue to mitigate this issue by converting waste materials into functional components for soil stabilization (Babu & Chouksey, 2011).

PWG functions mainly through mechanical reinforcement rather than chemical reaction. When mixed with clay soils, the granules act as miniature reinforcing fibers, forming a network that restrains deformation and distributes stresses more uniformly. This mechanism improves ductility, tensile strength, and resistance to cracking and settlement.

Research has shown that small additions of PWG (typically 0.5–3% by weight of dry soil) can lead to notable improvements in strength and CBR, particularly in clay soils used as foundation materials (Akinwumi et al., 2019; Onyelowe & Van, 2020). Beyond the engineering benefits, using PWG helps address environmental concerns by reducing the volume of non-biodegradable plastics that would otherwise persist in the environment for centuries.

By integrating PWG with reactive stabilizers such as CCR or lime, a more balanced improvement can be achieved chemical reactions contribute to stiffness, while PWG enhances flexibility and resilience. This synergy helps to overcome the brittleness commonly associated with chemical stabilization alone.

2.7 Previous Research on the use of CCR and PWG as Standalone or Binary or Ternary Combination with other Stabilizers

Calcium carbide residue (CCR) and plastic waste granules (PWG) have both been studied as alternative materials for soil stabilization, either on their own or combined with traditional stabilizers such as lime, cement, or fly ash.

Used alone, CCR has been shown to strengthen clayey and expansive soils because of its high calcium hydroxide content, which reacts with soil minerals to form cementitious compounds. This leads to noticeable improvements in unconfined compressive strength (UCS) and California Bearing Ratio (CBR), as well as reductions in plasticity and swelling, making soils more suitable for construction (Almuaythir et al., 2024; Luo et al., 2023). On the other hand, PWG works mainly through mechanical reinforcement rather than chemical reactions. Adding plastic granules to soil improves ductility, reduces brittleness, and increases resistance to tension and shear, helping soils better distribute loads in foundations and pavements (Babu & Chouksey, 2011).

Research on binary combinationspairing CCR or PWG with a conventional stabilizer like lime, cement, or fly ash shows even greater benefits. For example, CCR mixed with fly ash enhances soil strength more than CCR alone, thanks to stronger pozzolanic reactions. Similarly, combining PWG with lime or cement further reinforces the soil structure, reducing brittleness and improving toughness (Luo et al., 2023; Almuaythir et al., 2024).

Although studies on ternary blends involving CCR, PWG, and a traditional stabilizer are still limited, early research suggests these combinations could offer the best of both worlds. CCR provides chemical reactivity, while PWG adds mechanical reinforcement, producing a more balanced system that improves both strength and flexibility. Such blends could help overcome the brittleness associated with purely chemical stabilization while enhancing ductility and toughness (Luo et al., 2023).

Overall, these studies highlight the potential of CCR and PWG, whether used alone or in combination, as sustainable soil stabilizers. At the same time, they show that more research is needed on ternary mixtures, optimal proportions, and real-world field performance.

2.7.1 Synergistic Potential of CCR and PWG in Ternary Blends

The combined use of CCR and PWG provides a dual mechanism of soil improvement chemical and mechanical. CCR enhances chemical bonding and stiffness through pozzolanic reactions, while PWG reinforces the soil matrix mechanically, improving ductility and distributing loads. The combination results in a stabilized soil that is stronger, more resilient, and more durable than when either additive is used alone.

When lime is incorporated in small quantities, the resulting ternary blend (Lime + CCR + PWG) further enhances soil properties. Lime acts as a chemical initiator, CCR sustains the pozzolanic reactions, and PWG provides structural reinforcement. Studies by Olawale et al. (2023) and Madu et al. (2024) demonstrated that such ternary mixtures can achieve higher UCS and CBR values, alongside reduced swelling and improved durability, compared to single or binary blends.

Nevertheless, gaps exist in understanding the long-term performance of such ternary mixtures in foundation applications, as most prior studies have focused on pavement subgrades. This underscores the need for continued research, such as the present study, to establish the suitability of CCR–PWG–lime combinations for structural foundation stabilization.

2.7.2 Basis for Mix Design and Experimental Framework

The formulation of the mix design for this study is guided by findings from previous research and established engineering practice. Studies involving CCR have used between 4% and 12% by weight of dry soil, while PWG typically ranges from 0.5% to 3%. Lime is used in smaller amounts (2–6%) to initiate early chemical reactions while maintaining environmental and cost efficiency (Akinwumi et al., 2019, Mohammadi Darestani et al., 2025, Piechowicz et al., 2024).

The experimental framework for this study includes tests on both untreated and stabilized samples to evaluate changes in Atterberg limits, compaction characteristics, UCS, CBR, and durability under wet-dry cycles. These parameters are chosen to reflect both short-term improvements (strength and stiffness) and long-term performance (durability and stability).

This framework is designed for clay soils commonly found in Nigeria, where high plasticity and poor bearing capacity pose major challenges for foundation construction. The outcomes are expected to provide practical guidelines for sustainable and economical soil improvement.

2.8 Present Status of Research on Ternary Combination of Lime, CCR and PWG

Recent research in soil stabilisation has increasingly focused on the combined use of lime, calcium carbide residue (CCR), and plastic waste granules (PWG) as a sustainable alternative to conventional stabilising agents. This approach is driven by the need to improve weak soil performance while simultaneously addressing environmental concerns related to industrial and plastic waste disposal.

Lime has long been established as an effective soil stabiliser due to its ability to reduce plasticity and improve strength through cation exchange and pozzolanic reactions. Calcium carbide residue, a by-product of acetylene gas production, contains a high proportion of calcium hydroxide and has been shown to perform similarly to lime in alkaline activation. Studies indicate that CCR enhances soil strength and stiffness by increasing pH and supplying calcium ions that promote the formation of cementitious compounds such as calcium silicate hydrate (C–S–H) and calcium aluminate hydrate (C–A–H).

Plastic waste granules, on the other hand, act primarily as a mechanical reinforcement material rather than a chemical binder. Research on PWG in soil stabilisation has shown that discrete plastic particles improve ductility, tensile resistance, and post-peak behaviour of treated soils. The inclusion of PWG reduces brittleness, limits crack propagation, and enhances energy absorption, particularly under loading conditions relevant to pavement subgrades and embankments.

Although the individual and binary effects of lime–CCR and lime–plastic waste systems have been widely studied, investigations into their ternary combination remain limited. Available studies suggest that the combined use of lime and CCR provides a highly alkaline environment that accelerates pozzolanic reactions, while PWG contributes to structural reinforcement by bridging soil particles and improving stress distribution within the matrix. This synergy results in improved unconfined compressive strength, California Bearing Ratio, and durability compared to untreated soil or soil treated with a single additive.

Current research trends highlight the potential of ternary lime–CCR–PWG systems to produce stabilized soils with enhanced strength and deformation characteristics while significantly reducing reliance on traditional cementitious materials. However, gaps still exist regarding optimal mix proportions, long-term durability, environmental performance, and field-scale validation. Further experimental and mechanistic studies are therefore required to fully establish design guidelines for practical engineering applications.

CHAPTER THREE

MATERIALS AND METHODS

This chapter covers the methods used for collection of materials, laboratory testing for the untreated and treated soil samples. Conventional tests for evaluation of soil suitability for engineering purposes were carried out on the samples collected from the site and were treated with the stabilizers subsequently.

3.1 Sampling of Materials

The materials used for this research include; soil, lime, plastic waste granules, calcium carbide residue.

3.1.1 Clay Soil

The soil sample was gotten from Odo Ado, Ado-Ikare road, Ado Ekiti, Ekiti Nigeria (latiude 7.602599, longitude 5.317619). The clay soil was collected at depth of between 0.5m – 1.5m using the method of disturbed sampling. The clay soil was then air-dried and pulverized and the geotechnical properties of the soil were determined in the laboratory.

3.1.2 Lime

The lime used as a chemical additive for this study is hydrated lime. It was sourced from local suppliers in Ado, Ekiti State.

3.1.3 Calcium Carbide Residue

The CCR used was collected from automobile shops within Ado, Ekiti State, Nigeria. This area contains a lot of calcium carbide residue waste which is usually disposed haphazardly.

3.1.4 Plastic Waste Granules

PET bottles were collected around Iworoko, Ekiti state, it was shredded, washed and milled into fine particles.

3.2 Experimental Programme

The experimental programme was structured to systematically evaluate the influence of ternary blends of hydrated lime (L), calcium carbide residue (CCR), and plastic waste granules (PWG) on the engineering behavior of high-plasticity soil. Tests were grouped into index property, compaction, strength. All procedures adhered to ASTM, AASHTO, or BS standards unless otherwise specified.

3.2.1 Natural Clay Soil

Collection of soil was conducted using disturbed methods to obtain samples from depths of 0.5-1.5 m, following Nigerian General Specifications (Section 6100) for disturbed sampling (Federal Republic of Nigeria, 1997).

Preliminary tests (such as Atterberg limits, Specific Gravity, Grain size distribution, Standard compaction test, California bearing ratio and Unconfined compression test) for the purpose of determining the soil’s index properties were carried out on the sample according to the BS 1377 part 2: 1992 of the British Standard code.

3.2.2 Stabilized Soil

3.2.1 Sample Preparation

Soil was air-dried, pulverized, and sieved through No. 4 sieve (4.75 mm). Stabilizers were added by dry weight in accordance to the mix ratio as shown in Table 3.1, mixed uniformly using a mechanical mixer for 15 minutes (ASTM D5102, 2018).

Tests on stabilized soil:

- Atterberg limits

- Standard compaction test

- California bearing ratio (CBR) test

- Unconfined compression (UCS) test

Table 3.1 Mixture and their Acronyms

| S/N | SAMPLE MIX | SAMPLE DESCRIPTION |
| --- | --- | --- |
| 1. | SOIL + 6% L | L6 |
| 2. | SOIL + 6%L +1% CCR | L6-C1 |
| 3. | SOIL + 6%L +1% CCR + 0.5%PW | L6-C1-P0.5 |
| 4. | SOIL + 6%L +1% CCR + 1%PW | L6-C1-P1 |
| 5. | SOIL + 6%L +1% CCR + 1.5%PW | L6-C1-P1.5 |
| 6. | SOIL + 6%L +1% CCR + 2%PW | L6-C1-P2 |
| 7. | SOIL + 6%L + 2%CCR | L6-C2 |
| 8. | SOIL + 6%L +2% CCR + 0.5%PW | L6-C2-P0.5 |
| 9. | SOIL + 6%L +2% CCR + 1%PW | L6-C2-P1 |
| 10. | SOIL + 6%L +2% CCR + 1.5%PW | L6-C2-P1.5 |
| 11. | SOIL + 6%L +2% CCR + 2%PW | L6-C2-P2 |

3.3Laboratory Experimental Procedures

3.3.1 Specific Gravity Test

The specific gravity of the soil was determined using the density bottle method. Prior to testing, the soil sample was passed through a 5.0 mm British Standard (BS) sieve to remove deleterious materials and ensure uniformity. The density bottle was first cleaned, dried, and weighed empty, and this mass was recorded as M1. A representative portion of the sieved, oven-dried soil was then placed into the bottle, and the combined mass of the bottle and dry soil was recorded as M2​.

Distilled water was gradually added to the bottle until it reached the calibration (gauge) mark, after which the contents were allowed to soak. The bottle was gently shaken to eliminate entrapped air and surface bubbles, ensuring complete saturation of the soil particles. The mass of the bottle containing dry soil and water was then recorded as M3. Subsequently, the bottle was emptied, thoroughly cleaned, and dried. It was then filled with distilled water only up to the gauge mark, and the mass was recorded as M4.

The specific gravity of the soil (Gs) was calculated as the ratio of the weight of the dry soil sample to the weight of an equal volume of water, using the expression:

The specific gravity (Gₛ)=weight of dry sampleweight of equal volume of water

The specific gravity (Gₛ)=M2 - M1 (M4 - M1) - (M3 - M2)

3.3.2 Grain Size Distribution

Grain size distribution (GSD) refers to the relative proportions of different particle sizes present in a soil mass. It is a fundamental index property used for soil classification and for predicting engineering behavior such as permeability, shear strength, compressibility, and compaction characteristics (Das & Sobhan, 2018). GSD is commonly determined using sieve analysis for coarse-grained soils and hydrometer analysis for fine-grained soils.

### Sieve Analysis

Sieve analysis is used to determine the particle size distribution of coarse-grained soils, such as gravel and sand. The test involves passing a dry soil sample through a series of standard sieves arranged in descending order of aperture size. The mass of soil retained on each sieve is measured and expressed as a percentage of the total sample weight (ASTM International, 2017a).

The results are used to plot a grain size distribution curve on a semi-logarithmic scale, which aids in soil classification and in assessing whether the soil is well-graded, poorly graded, or uniformly graded (Das & Sobhan, 2018).

### B. Hydrometer Analysis

Hydrometer analysis is used for fine-grained soils, particularly silts and clays, whose particle sizes are too small to be measured by sieving. This method is based on the principle of sedimentation, which is governed by Stokes’ law. Stokes’ law states that the settling velocity of soil particles in a fluid is proportional to the square of their diameter (Craig, 2004).

A hydrometer is used to measure the density of the soil-water suspension at specified time intervals, from which particle sizes and their corresponding percentages are computed (ASTM International, 2017b). This test provides essential information on the distribution of fine particles, which strongly influences the plasticity, compressibility, and permeability of soils.

The particle size distribution of the soil was determined in accordance with BS 1377 Part 2: 1992. To isolate the clay fraction, the soil sample was first washed through a 0.075 mm sieve, and the retained material was oven-dried at 105 °C for 24 hours. This dried sample was then riffled to obtain a representative portion of approximately 200 g, which was subjected to mechanical sieve analysis using a stack of standard BS sieves ranging from 5.0 mm to 0.075 mm. The stack was placed on a mechanical shaker and agitated for 10 minutes. After sieving, the mass of soil retained on each sieve was recorded to the nearest 0.1 g.

The percentage retained on each sieve was calculated as:

% Retained=mass retained on sieve total dry mass of sample× 100

The cumulative percentage retained was summed progressively from the largest sieve downward, and the percentage passing each sieve was obtained as:

% Passing = 100 − cumulative % retained

A particle size distribution curve was plotted on a semi-logarithmic graph, with particle diameter (mm) on the logarithmic x-axis and percentage passing on the arithmetic y-axis. From this curve, the characteristic grain sizes D₁₀, D₃₀, and D₆₀ were determined graphically.

The percentage of clay-sized particles was calculated from the washed fraction as:

% Clay=mass of material passing 0.075mm sieve total initial dry mass× 100

The coefficient of curvature (C₍c₎) and coefficient of uniformity (C₍u₎) were computed using:

C₍c₎ =(D₃₀)² (D₁₀ × D₆₀)

C₍u₎ = D₆₀ D₁₀

A soil is classified as well-graded if 1 < C₍c₎ < 3 and C₍u₎ > 6 (for sands) or C₍u₎ > 4 (for gravels). If C₍u₎ < 4, the soil is considered poorly graded or uniformly graded. For single-sized material, both C₍u₎ and C₍c₎ equal 1. Any soil with more than 35% passing the 0.075 mm sieve is generally deemed unsuitable for use as subgrade or fill unless improved, depending on its plasticity characteristics; in such cases, replacement with better-quality material is preferred, or the soil may be stabilized.

3.3.3 Atterberg limits

Liquid Limit

The liquid limit (LL) is the water content at which a soil changes from a plastic state to a liquid state. At this moisture content, the soil begins to flow under its own weight and exhibits very low shear strength. The liquid limit is commonly determined using the Casagrande cup method or the cone penetrometer method (ASTM International, 2017a).

LL is an important parameter for soil classification and provides insight into the compressibility, permeability, and swelling potential of fine-grained soils (Craig, 2004).

Plastic Limit

The plastic limit (PL) is the water content at which soil changes from a semi-solid state to a plastic state. It is determined by rolling soil threads until they crumble at a diameter of approximately 3 mm (ASTM International, 2017a).

The difference between the liquid limit and plastic limit is known as the plasticity index (PI), which indicates the range of moisture content over which the soil remains plastic. Soils with high PI values tend to exhibit greater compressibility and volume change behavior (Das & Sobhan, 2018).

Linear Shrinkage

Linear shrinkage (LS) refers to the reduction in length of a soil specimen as it dries from its liquid limit state to the oven-dried condition. It is expressed as a percentage of the original length. This test provides an indication of the shrinkage potential of soils, particularly clays (BS 1377, 1990).

Soils with high linear shrinkage values are more susceptible to cracking, settlement, and volume changes due to moisture variation, which can adversely affect pavement and foundation performance (Craig, 2004).

The Atterberg limits were determined per BS 1377 Part 2: 1990 to classify the soil. The liquid limit (LL) was the moisture content at 25 blows on the flow curve; the plastic limit (PL) was the average moisture content when a 3 mm thread crumbled. Plasticity index (PI) = LL – PL. Moisture contents were measured by oven drying at 105 °C for 24 hours. Tests were run in duplicate, accepting LL differences < 2% and PL differences < 1%. The soil classified as CL (USCS), CI (British), and A-7-6 (AASHTO). With PI > 10 and > 35% passing No. 200 sieve, stabilization was required.

The Atterberg limits of the soil were determined using the Casagrande apparatus in accordance with standard procedures. For the liquid limit test, approximately 200 g of soil passing the 425 µm sieve was mixed with distilled water to form a uniform paste. The prepared paste was placed into the Casagrande cup, and a standard groove was cut along the center using the grooving tool. The cup was then repeatedly dropped at a rate of about two blows per second until the two halves of the soil paste came into contact along a length of 13 mm. The number of blows required to achieve this closure was recorded, and a representative sample was taken immediately for moisture content determination.

The test was repeated several times at different moisture contents, producing blow counts typically ranging between 15 and 35. A flow curve was established by plotting the moisture content against the logarithm of the corresponding number of blows. The liquid limit (LL) was obtained from this curve as the moisture content corresponding to 25 blows.Top of Form

Bottom of Form

The plastic limit (PL) obtained from the analysis of the data from the plastic limit test.

The plasticity index of the soil was calculated as shown in equation:

Plasticity index (PI) = Liquid Limit (LL) – Plastic Limit (PL)

The liquid limit and plasticity index values obtained from the Atterberg limits test were used to classify the soil. According to the Unified Soil Classification System (USCS), the soil is designated as low-plasticity clay (CL). Under the British Soil Classification System, it is classified as intermediate-plasticity clay (CI). In the American Association of State Highway and Transportation Officials (AASHTO) system, the soil falls into the A-7-6 category. With a plasticity index exceeding 10 and more than 35% of the material passing the No. 200 sieve, the soil is considered weak, necessitating stabilization to lower plasticity and enhance strength.

3.3.4 Standard Compaction Test

The compaction test was conducted per BS 1377 (1992) using the British Standard Heavy (Modified) method to define the dry density–moisture content relationship for the soil as foundation material. A 1000 cm³ cylindrical mould (101.6 mm internal diameter, 116.43 mm height) with base plate and 50 mm collar was used, along with a 4.5 kg rammer (50 mm face) falling 450 mm. Compaction was applied in three layers with 25 blows each.

The procedure was:

The compaction characteristics of the soil were determined using the standard Proctor compaction test. Approximately 3000 g of air-dried soil was first pulverized in a mixing tray to break down soil aggregates and ensure uniformity. An initial water content of about 6% by dry weight of soil was added, and the mixture was thoroughly blended to obtain a homogeneous mass.

The prepared soil was placed into the compaction mould in three equal layers. Each layer was compacted by applying 25 uniform blows using the standard rammer to ensure consistent energy input. After compaction, the mould and its contents were weighed to determine the bulk density. The compacted soil specimen was then carefully extruded from the mould, and representative samples were taken from the top and bottom portions of the specimen. These samples were oven-dried at 105 °C to determine the moisture content, which was subsequently used in calculating the dry density.

Following this, the soil was repulverized, and additional water was added in increments of approximately 3% by dry weight. The compaction procedure was repeated for each moisture content until a reduction in bulk density was observed in two consecutive tests, indicating that the maximum compaction condition had been exceeded. A compaction curve was then developed by plotting dry density against moisture content. The peak of this curve was used to determine the maximum dry density (MDD), while the corresponding moisture content was identified as the optimum moisture content (OMC).

Dry density:

DD (g/cm³) =  Dₙ(1 + MC/100)

Wet density: Dₙ (g/cm³) =  Wₛ Vₛ

OMC must not exceed 18% (Federal Ministry of Works and Housing, 1997) to ensure bearing capacity and control settlement.

3.3.5 California Bearing Ratio (CBR) Test

The California Bearing Ratio (CBR) test was conducted in accordance with BS 1377 Part 2: 1992 to evaluate the soil’s bearing capacity.

CBR was calculated as:

CBR (%) = (Test load Standard load )× 100

Test load (kN) = Load reading × 0.0416

CBR at 2.5 mm = (Reading × 0.0416  13.24) × 100

CBR at 5.0 mm = (Reading ×  0.0416 19.96) × 100

Procedure:

The California Bearing Ratio (CBR) test was conducted to evaluate the load-bearing capacity of the soil at its optimum moisture condition. Approximately 6000 g of air-dried soil was first weighed and thoroughly mixed with water to achieve the previously determined optimum moisture content (OMC), ensuring uniform distribution of moisture and preventing segregation.

The CBR mould was then assembled with the base plate and collar, and the prepared soil was placed into the mould in five equal layers. Each layer was compacted using 62 blows of a 4.5 kg rammer falling freely through a height of 450 mm. To ensure adequate bonding between successive layers, the surface of each compacted layer was lightly scarified before placing the next layer. After compaction was completed, the collar was removed, and the excess soil was carefully trimmed flush with the top of the mould. The mass of the mould containing the compacted specimen was recorded.

The mould and specimen were then positioned on the CBR testing machine, and a surcharge weight of 10 kg was placed on the specimen to simulate pavement overburden. The penetration plunger was seated centrally on the soil surface, and penetration was applied at a constant rate of 1.25 mm per minute. Proving ring readings were recorded at penetration intervals of 0.5 mm up to a maximum penetration of 12.5 mm.

The California Bearing Ratio values were calculated at penetrations of 2.5 mm and 5.0 mm. In accordance with standard practice, the higher of the two calculated CBR values was selected and reported as the CBR of the soil specimen.

3.3.6 Unconfined Compression (UCS) Test

The Unconfined Compressive Strength (UCS) represents the peak axial stress a cylindrical cohesive soil specimen sustains under zero lateral confinement. It is calculated as the failure load divided by the cross-sectional area and serves as a reliable indicator of stabilized soil strength (Das, 2010). UCS tests on stabilized samples followed BS 1377 Part 7: 1990 and NGS (1997).

The procedure was as follows:

The unconfined compressive strength (UCS) test was carried out on a compacted soil specimen to determine its shear strength under unconfined conditions. The large compacted sample was first extruded using a sampling tube, and the soil contained within the tube was saturated where required. A split mould was then lightly greased and weighed empty before being filled by directly extruding the soil from the sampling tube into the mould. Excess soil at both ends of the mould was carefully trimmed to obtain smooth, flush surfaces.

The mould containing the specimen was weighed, after which the specimen was gently removed by splitting the mould to avoid disturbance. The length and diameter of the specimen were measured accurately using a Vernier caliper, and the specimen was then positioned centrally between the platens of the compression testing machine. The dial gauge and proving ring were set to zero, and proper contact between the upper platen and the specimen was ensured before loading commenced.

Axial load was applied at a constant strain rate, and readings of axial deformation and corresponding load from the proving ring were recorded at 25-second intervals. Loading was continued until a clear shear failure of the specimen was observed. After failure, the angle of the failure plane with the horizontal was noted, and a representative soil sample was collected from the failure zone for determination of the moisture content.

UCS was computed as:

UCS (kPa) = Failure load (N) Cross-sectional area (mm²)

CHAPTER FOUR

RESULT AND DISCUSSION

4.1 ENGINEERING PROPERTIES OF THE NATURAL SOIL

The specific gravity of the soil, which is an index of its density, is 2.46. This is also within the expected limits for a clay soil that can be found in tropical areas like Nigeria which ranges from 2.40-2.60(Sorsa et al., 2020, Andre-Obayanju et al., 2022). The other parameter that defines the particle size distribution of the soil shows that the material is dominated by fine grains to a larger extent, with a value of 51.30% for the silt and clay size fraction and 48.70% for the coarse fraction. The coarse fraction has 33.60% sand and 15.06% gravel. The consistency index for the soil defines its other properties to have a value of 56.50% for the liquid limit, with a plastic limit of 31.18%, thus producing a value for the plastic index of 25.32%. The material is therefore medium to high in plastic index values. The linear shrinkage of 7.86% also points towards the possible presence of clay, which can be problematic due to its possible volume changes. All other physical and chemical properties can be seen in Table 4.1.

Compaction characteristics of the soil have a maximum dry density (MDD) of 1781 kg/m³ at an optimum moisture content (OMC) of 15%. It is an indication that the compaction ability is not very high. The coefficient of curvature (Cc) of 1.45 and a coefficient of uniformity (Cu) of 319.23. This shows that it will be a well-graded soil. Additionally, the soaked CBR value of 14.25% indicates that the soil exhibits moderate subgrade strength, meaning it can support light to medium traffic loads but may require appropriately designed base and sub-base layers to prevent excessive deformation under heavier loads (Bowles, 1996). Though this value might not be ideal for heavy highways for unimproved pavements (ASTM D1883, 2016).

According to the AASHTO soil classification system, the soil is identified as group A-7-5(10), indicating that it is of fair to poor subgrade material. Likewise, the USCS classification system groups the soil as MH, an identification that refers to inorganic silt of high plasticity. In conclusion, the level of identification of the soil under the two systems reveals that the soil is not directly suitable for construction. Thus, there is a need for soil improvement as a method of improving its properties for construction.

Table 4.1 Physical and chemical properties of the soil

| Properties of soil | Soil sample |
| --- | --- |
| Specific gravity | 2.46 |
| Percentage of coarse | 48.7% |
| Percentage of silt & clay | 51.30% |
| Percentage of gravel | 15.06% |
| Percentage of sand | 33.64% |
| Liquid limit(%) | 56.50 |
| Plastic limit (%) | 31.18 |
| Linear shrinkage | 7.86% |
| Plasticity index (%) | 25.32 |
| Maximum dry density (kg/m3) | 1781 |
| Optimum moisture content (%) | 15% |
| Coefficient of curvature, Cc | 1.45 |
| Coefficient of uniformity, Cu | 319.23 |
| California bearing ratio (%) | 14.23 |
| AASHTO Classification | A-7-5(10) |
| USCS | MH |

Fig 4.1: Particle size distribution curve of natural soil sample

4.2 EFFECT OF CONSISTENCY LIMITS OF STABILIZED SOIL

The study on behavior of consistency limits of stabilized soil adds three factors through the use of lime (L), calcium carbide residue (CCR), and plastic waste (PW). The plasticity of stabilized soil is observed, and there is a general increase in the value of liquid limit (LL) and plastic limit (PL) of soil with stabilization. Variations occur in plasticity index (PI) on stabilization. Initially, natural soil contains LL=56.50%, PL=31.18%, and PI=25.32%. When it is treated with 6% lime (L6), it shows substantial reduction in PI to 10.91%, thus showing good improvement in its plasticity properties.

The rise in both LL and PL can be attributed to the displacement of soil particles by the stabilizers, as well as the flocculation-agglomeration reaction triggered by both lime and CCR. Despite the fact that both lime and CCR are recognized as pozzolanic/calcium stabilizers, their interaction with clay can be attributed to the production of cementing products, which enhance soil structuring. Similar results were reported by Bell (1996), which attributed the rise in both liquid and plastic limits in lime-treated soils to soil structuring-soil mineralogy changes.

The reduction in PI observed in some of the stabilized samples may be due to the hydration and pozzolanic reactions between the additives and the soil, which ultimately result in the formation of a stiffer and more stable soil mixture (Tang et al., 2025.). Among all the stabilized mixes, the L6 blend exhibited the best plasticity performance with the lowest PI value of 10.91%, indicating a significant reduction in soil plasticity which is not a surprise because of the use of lime as a conventional method for stabilization but looking at L6-C1-P1 it is noticed that the PI is lesser than that of the natural soil. This reduction in PI implies improved workability, reduced swelling potential, and better volumetric stability of the stabilized soil (Ayodele et al., 2022, Miedema, 2021, Waleed & Alshawmar, 2025) Figure 4.3 shows the results of the effects of lime–CCR–plastic waste stabilization on the stabilized soil.

Fig 4.2: consistency limit behavior of stabilized soil

4.3 Effect of lime–CCR–plastic waste on the compaction characteristics of the stabilized soil

The compaction behaviour of the lime-CCR-plastic waste stabilized soil showed that the MDD upon addition of varying mixes (L6%, C 1-2%, P 0.5-2%) was lowered compared to the natural soil except mix L6 & L6-C1-P0.5 which were higher than that of the natural soil. The compaction chart showing the MDD and OMC generated as a result of the stabilization are shown in Fig. 4.3. There was a general decrease in MDD except mix L6 and L6-C1-P0.5. It was noticed that L6 has higher MDD than the natural soil (1821 Kg/m >1781 Kg/m) there is also increase in MDD for the mix L6-C1-P0.5(1802 Kg/m) and this may be due to the cementitious properties of the lime for mix L6 and for mix L6-C1-P0.5. The OMC increased with the addition of the admixes due to the increase in fines from the stabilizers with larger surface areas that required more water for hydration.

Fig 4.3: compaction chart for Lime-Calcium Carbide Residue-Plastic Waste Granules

4.4 Effect of lime CCR and plastic waste, on the strength of the stabilized soil

Unconfined compressive strength (UCS) helps find the right number of hard mixtures, for good soil stabilization. Looking at the UCS test results It is observed that adding the lime, CCR and the plastic waste made the stabilized soil much stronger as shown in Fig 4.4. The natural soil recorded a UCS value of 147.53 kN/m², while the stabilized mixtures generally exhibited higher strength values, with the peak strength observed at the L6-C2-P0.5 blend, which recorded 213.11 kN/m². The UCS values gotten are from 3 days curing exercise.

From the graph it is observed that the strength goes up because of cementitious compounds form when lime and CCR react with water. The pozzolanic reactions produce calcium silicate hydrates (CSH) and calcium aluminate hydrates (CAH). CSH and CAH bind the soil particles together making the bonds stronger. Plastic waste filled the void, stop particle movement, it makes the soil matrix stronger which also increases the load‑bearing capacity of the stabilized soil. Similar behavior was reported by Attom et al. (2025), who observed that chemical stabilization significantly improves soil strength due to microstructural modification and cementation.

Mix L6-C2-P0.5 recorded the highest UCS, the chemical and physical properties of lime and CCR enhance strength by promoting pozzolanic reactions, reducing water demand, and improving particle interlocking. However, beyond this mix(L6-C2-P0.5), additional stabilizer can disrupt particle packing and reduce densification efficiency, resulting in lower strength gains. This pattern of peak strength at 6% lime, 2% CCR and 0.5% PWG followed by diminished performance at higher contents has been widely reported in recent soil stabilization studies (Baldovino et al.2024).

Overall, the results indicate that stabilization significantly enhanced the strength characteristics of the soil, making it more suitable for engineering applications. Figure 4.4 illustrates the effects of lime–CCR–plastic waste stabilization on the UCS behavior of the clay soil.

Fig 4.4: UCS chart for Lime-CalciumCarbideResidue-PlasticWasteGranules.

4.5 Effect of Lime, CCR and PWG on California Bearing Ratio (CBR) of the Stabilized Soil

The California Bearing Ratio (CBR) values of subgrade, sub‑base and base materials are important, in pavement design. The CBR values directly set the thickness (Amakye et al., 2022). Figure 4.5 shows the CBR behavior of the stabilized soil. The natural soil produced a CBR value of 14.23 percent, Soils with CBR values between 5% and 15% are considered to have moderate subgrade strength (Bowles, 1996; Amakye et al., 2022). With stabilization, the CBR values generally showed slight improvement and fluctuation depending on the blend proportions. For the soil mix with 6% lime the CBR value was recorded as 14.31percent slightly higher than that of the natural soil. Adding CCR and plastic waste raised the CBR value a little. The highest CBR value of 15.72 percent occurred in the L6‑C1‑P0.5 mix. The next highest CBR value of 15.58 percent occurred in the L6‑C2‑P1.5 mix. The results show that adding amounts of plastic waste granules, CCR and lime increased the load‑bearing capacity of the clay soil, this may be due to pozzolanic reactions of CCR, forming cementitious bonds between soil particles while plastic granules occupy voids and reinforce the soil matrix. However, a reduction in CBR was observed, as seen in samples such as L6-C1-P2 (14.01%) and L6-C2 (13.59%). This reduction may be due to excess stabilizer content, which can lead to incomplete bonding and reduced interparticle friction.

The increase in CBR values is due to the cementitious reactions between lime and CCR, which form calcium silicate hydrates (CSH) and calcium aluminate hydrates (CAH) that bind soil particles and reduce voids (Akula & Little, 2020). Plastic waste further improves strength by restricting particle movement under load. According to AASHTO and other highway standards, soils with soaked CBR values above 5–8% are suitable for subgrade use. Since all stabilized samples exceeded this range, they are suitable as subgrade materials. The L6–C1–P0.5 mix showed the best performance, achieving the highest CBR of 15.72%.

Fig 4.5: CBR chart for Lime-CCR-PWG.

CHAPTER FIVE

5.1 CONCLUSION

Following the stabilization of the soil with the ternary blend of lime, calcium carbide residue (CCR), and plastic waste (PW) the following conclusions are drawn:

1. The soil is fine grained, characterized as MH and A-7-5(10) according to the USCS and AASHTO soil classification system.

2. The natural soil had LL, PL and PI of 56.50%, 31.18% and 25.32% respectively and with the inclusion of Lime, CCR and PWG, there was a significant increase in LL and PL with PI also showing a significant increase except mixes L6 and L6-C2-P1.

3. The stabilized soil recorded a significant decrease in MDD except from mixes L6 and L6-C1-P0.5 and there was also significant increase in the OMC values due to the increase in fines from the stabilizers with mix L6-C2-P2 having the highest value.

4. The natural soil had low strength (UCS = 147.53 kN/m²). The inclusion of lime, CCR and PWG after 3 days of curing increased the UCS significantly with mix L6-C2-P0.5 having the highest value (213.11 KN/ m²).

5. The natural soil had a moderate CBR of 14.23%. Stabilization slightly improved strength as there was a general increase in the CBR except mixes L6-C1-P2 and L6-C2. The highest CBR is 15.72% for the mix L6–C1–P0.5. All mixes met subgrade requirements.

6. Consistency limits, UCS, and CBR results confirm that stabilization improved the soil’s properties.

5.2 RECOMMENDATION

The following recommendation are hereby made based on the results.

1. The blends L6–C2–P0.5 (6% lime, 2% Calcium carbide residue and 0.5% Plastic waste granule) and L6–C1–P0.5 (6% Lime, 1% Calcium carbide residue and 0.5% Plastic waste granules) can be adopted for stabilizing plastic inorganic silty soils, mix L6-C2-P0.5 is suitable to improve soil with low UCS and mix L6-C1-P0.5 is recommended to improve soil low CBR. They demonstrated the best overall performance in terms of reduced plasticity, improved strength, and enhanced bearing capacity.

2. The validated improvements in consistency limits, UCS, and CBR confirm the effectiveness of this stabilization technique for subgrade applications. Furthermore, the use of industrial waste materials should be promoted, and the reliance on lime can be minimized or jettisoned where these optimal blends are applied.

3. Future studies should be done on the long term effect of these ternary blend as well as a field observation.

REFERENCE

AASHTO. (1993). Guide for Design of Pavement Structures. American Association of State  	Highway and Transportation Officials, Washington, DC.

Ahmadullah, T., & Chrysochoou, M. (2024). Relationship between strength development and 	pozzolanic reactions in lime stabilized kaolinite. International Journal of Geo-Engineering, 	15(1), 11.

Andre-Obayanju, O., Edegbai, A. J., & Imarhiagbe, O. J. (2022). Geotechnical Properties of Some 	Clay Deposits in Some Parts of Southwestern Nigeria in Relation to Its Engineering 	Implications on Constructions. Bilingual Publishing Co, 4(3).

Alqawasmeh, H. M. (2025). Enhancing the sustainability of geotechnical engineering with 	utilization of fly Ash. Discover Materials, 5(1), 11.

Al-Bakri, A. Y., Ahmed, H. M., & Hefni, M. A. (2022). Cement kiln dust (CKD): potential 	beneficial applications and eco-sustainable solutions. Sustainability, 14(12), 7022.

Al-Mukhtar, M., Khattab, S., & Alcover, J. F. (2014). Microstructure and geotechnical behavior 	of lime-treated expansive clay soils. Engineering Geology, 168, 1–13.

Almuaythir, S., Zaini, M. S. I., Hasan, M., & Hoque, M. I. (2024). Sustainable soil stabilization 	using industrial waste ash: Enhancing expansive clay properties. Heliyon, 10(20).

ASTM D559. (2015). Standard test methods for wetting and drying compacted soil–cement 	mixtures. ASTM International.

Al-Chaer, A., & Hamadneh, A. (2025). Soil improvement using plastic waste–cement mixture to		 control swelling and compressibility of clay soils. Buildings, 15(8), 1387. 	https://doi.org/10.3390/buildings15081387

Akula, P., & Little, D. N. (2020). Analytical tests to evaluate pozzolanic reaction in lime stabilized 	soils. MethodsX, 7, 100928.

Anjum, S., Sharma, A., Onyelowe, K. C., Alsabhan, A. H., Alam, S., Singh, K., ... & Qadri, J. 	(2025). Sustainable subgrade improvement with calcium carbide residue and rice husk ash. 	Scientific Reports, 15(1), 14351.

Animashaun, L., Yekinni, A., Olaiya, K., Ogunyemi, O., & Adewuyi, P. (2025). Estimation of 	plastic production, consumption, and waste generation in Nigeria: 2020 to 2050. 	Environmental Research and Technology, 8(4), 784-791.

Akeem, A. A., Olayinka, O. O., & Yusuf, K. T. (2023). Sustainable approaches to soil stabilization	 using industrial and plastic wastes: A review. Journal of Environmental geotechnics, 	10(3), 245–258.

Awadalseed, W., Zhao, H., Sun, H., Huang, M., & Liu, C. (2023). Expansive soil stabilization by 	bagasse ash in partial replacement of cement. Journal of Renewable Materials, 11(4), 1911.

Amadi, A. A., & Okeiyi, A. (2017). Assessment of lime-stabilized lateritic soil for road pavement	construction. Journal of Materials in Civil Engineering, 29(7), 04017061.

Amadi, A. A., Edeh, J. E., & Okorie, U. (2019). Use of ground-granulated blast-furnace slag for 	stabilization of clay soils in Nigeria. Nigerian Journal of Technology, 38(2), 282–290.

Akula, P., & Little, D. N. (2020). Analytical tests to evaluate pozzolanic reaction in lime stabilized 	soils. MethodsX, 7, 100928.

ASTM International. (2017a). Standard test methods for particle-size distribution (gradation) of 	soils using sieve analysis (ASTM D6913). ASTM International.

ASTM International. (2017b). Standard test method for particle-size distribution (gradation) of 	fine-grained soils using the sedimentation (hydrometer) analysis (ASTM D7928). ASTM 	International.

ASTM D1586. (2017). Standard test method for standard penetration test (SPT) and split-barrel 	sampling of soils. ASTM International.

ASTM D5102. (2018). Standard test method for unconfined compressive strength of compacted     	 soil-lime mixtures. ASTM International.

ASTM D559. (2015). Standard test methods for wetting and drying compacted soil-cement 	mixtures. ASTM International.

Ayodele, F. O., Fajimi, M. S., & Alo, B. A. (2022). Stabilization of tropical soil using calcium 	carbide residue and rice husk ash. Materials Today: Proceedings, 60(Part 1), 216–222. 	https://doi.org/10.1016/j.matpr.2021.12.465

Attom, M., Al-Asheh, S., Yamin, M., Vandanapu, R., Al-Lozi, N., Khalil, A., & Eltayeb, A. 	(2025). Soil improvement using plastic waste–cement mixture to control swelling and 	compressibility of clay soils. Buildings, 15(8), 1387. 	https://doi.org/10.3390/buildings15081387

Anjum, S., Sharma, A., Onyelowe, K. C., et al. (2025). Sustainable subgrade improvement with 	calcium carbide residue and rice husk ash. Scientific Reports, 15, 14351. 	https://doi.org/10.1038/s41598-025-98833-z

Blayi, R. A., Kakrasul, J. I., & Hamad, S. M. (2025). An overview of rice husk ash as a waste by-	product material for sustainable soil stabilization. Cleaner Waste Systems, 100446.

Babu, G. L. S., & Chouksey, S. K. (2011). Stress–strain response of plastic-waste-mixed soil. 	Waste Management, 31(3), 481–488.

Baldovino, J. A., Nuñez de la Rosa, Y. E., & Namdar, A. (2024). Sustainable cement stabilization 	of plastic clay using ground municipal solid waste: enhancing soil properties for 	geotechnical applications. Sustainability, 16(12), 5195. 	https://doi.org/10.3390/su16125195

Bawab, J., El-Hassan, H., El-Dieb, A., Khatib, J., & El-Mir, A. (2025). Utilization of calcium 	carbide residue as a concrete component: A comprehensive review. Case Studies in 	Construction Materials, e04823.

Bell, F. G. (1993). Engineering treatment of soils. E & FN Spon.

Behnood, A. (2018). Soil and clay stabilization with calcium-and non-calcium-based additives: A 	state-of-the-art review of challenges, approaches and techniques. Transportation 	Geotechnics, 17, 14-32.

British Standards Institution. (1992). BS 1377-2:1992. Methods of test for soils for civil 	engineering purposes – Part 2: Classification tests. BSI.

Bell, F. G. (1996). Lime stabilization of clay minerals and soils. Engineering Geology, 42(4), 223–	237.

Bowles, J. E., & Guo, Y. (1996). Foundation analysis and design (Vol. 5, p. 127). New York: 	McGraw-hill.

Cai, D., Ouyang, M., Bao, X., Zhang, Q., Bi, Z., Yan, H., ... & Shi, Y. (2025). Performance 	evaluation of stabilized soils with selected common waste materials of rice husk ash, steel 	slag and iron tailing powder. Materials, 18(2), 346.

Craig, R. F. (2004). Craig’s soil mechanics (7th ed.). Spon Press.

Craig, R. F. (2012). Craig’s soil mechanics (8th ed.). CRC Press.

Consoli, N. C., Prietto, P. D. M., & Ulbrich, L. A. (2011). Influence of fiber and cement addition 	on behavior of sandy soil. Journal of Geotechnical and Geoenvironmental Engineering, 		124(12), 1211–1214.

Dansarai, M. M., Bawa, M. A., & Tokan, A. (2020). Nigerian Clay Deposits for use as Refractory 	Materials in Metallurgical Industries-A Review. International Journal of Engineering 	Research & Technology (IJERT), 9, 707-711.

Dash, S. K., & Hussain, M. (2012). A study on the performance of lime- and cement-stabilized 		clayey soils. International Journal of Civil Engineering, 10(4), 271–282.

Das, B. M., & Sobhan, K. (2017). Principles of geotechnical engineering (9th ed.). Cengage 	Learning

Das, B. M. (2010). Principles of geotechnical engineering (7th ed.). Cengage Learning.

Ettu, L. O., Opara, H. D., & Nwachukwu, C. C. (2013). Strength of lateritic soil stabilized with 	rice husk ash and cement for sub-base course construction. International Journal of 	Engineering and Science, 2(4), 39–44.

Etekume, C. (2020). Geotechnical Properties of Lateritic Soil Stabilized with Bone Ash and 	Hydrated Lime for Road Construction Applications (Doctoral dissertation).

Eriki, j. a. (2022). stabilisation of tropical soil with hydrated lime and plastic blend (doctoral 	dissertation).

Federal Ministry of Works and Housing. (1997). Nigerian General Specification for Roads and 	Bridges. Lagos: FMWH.

Federal Republic of Nigeria. (1997). General specification for roads and bridges. Abuja: 	Government Press.

Federal Highway Administration (FHWA). (2006). Soils and foundations reference manual 	(FHWA NHI-06-088). U.S. Department of Transportation.

Felix, N., & Raphael, D. S. (2025). Global Plastic Pollution and the Nigerian Dimensions. Journal 	of Geography, Environment and Earth Science International, 29(3), 26-42.

Gbadamosi, A. O. (2021). Geotechnical challenges of expansive soils in Nigeria: A review. 	African Journal of Engineering Research, 9(1), 12–20.

Geyer, R., Jambeck, J. R., & Law, K. L. (2017). Production, use, and fate of all plastics ever made. 	Science Advances, 3(7), e1700782.

Hassan, H.J.A., Rasul, J. & Samin, M. Effects of Plastic Waste Materials on Geotechnical 	Properties of Clayey Soil. Transp. Infrastruct. Geotech. 8, 390–413 (2021). 	https://doi.org/10.1007/s40515-020-00145-4

Hilaloglu, F., Kanwal, Q., Almarshoud, M. A., & Al-Ghamdi, S. G. (2026). CO₂ Sequestration 	Pathways in Cementitious Materials: Mechanisms, Material Synergies, and Deployment Challenges for Low-Carbon Construction. Resources, Conservation & Recycling Advances, 	200313

Horpibulsuk, S., Phetchuay, C., Chinkulkijniwat, A., & Cholaphatsorn, A. (2013). Strength 	development in silty clay stabilized with calcium carbide residue and fly ash. Soils and 	Foundations, 53(4), 477–486. https://doi.org/10.1016/j.sandf.2013.06.001Ingles, O. G., & 	Metcalf, J. B. (1972). Soil stabilization: Principles and practice. Butterworths.

Ige, O. E., Von Kallon, D. V., & Desai, D. (2024). Carbon emissions mitigation methods for 	cement industry using a systems dynamics model. Clean Technologies and Environmental 	Policy, 26(3), 579-597.

Kafinta, u. g. (2021). laboratory and field experimentation on the use of cement and calcium 	carbide residue for stabilization of lateritic soil (doctoral dissertation).

Kaothon, P., Lee, S.-H., Choi, Y.-T., & Yune, C.-Y. (2022). The effect of fines content on 	compressional behavior when using sand–kaolinite mixtures as embankment materials. 	Applied Sciences, 12(12), 6050. https://doi.org/10.3390/app12126050

Kamei, T., Ahmed, A., & Shibi, T. (2013). Laboratory investigation on the durability of cement-	stabilized soil. Soils and Foundations, 53(4), 597–609.

Komolafe, O. O., & Osinubi, K. J. (2019, November). Stabilization of lateritic soil with cement–	oil palm empty fruit bunch ash blend for California bearing ratio base course requirement. 	In IOP Conference Series: Materials Science and Engineering (Vol. 640, No. 1, p. 012085). 	IOP Publishing.

Little, D. N. (1995). Handbook for stabilization of pavement subgrades and base courses with lime. 	Kendall/Hunt Publishing Company.

Luo, X., Li, P., Ma, Z., Pei, Y., Ding, Z., Chen, R., & Fan, W. (2023). Investigation into the 	Enhancement Characteristics of Fly Ash and Polypropylene Fibers on Calcium Carbide-	Residue-Stabilized Soil. Sustainability, 15(23), 16360

Maneeth, P. D., Pramod, K., Kumar, B. R., & Shetty, S. (2014). Utilization of waste plastic in 	manufacturing of plastic-soil bricks. International Journal of Engineering Research & 	Technology (IJERT), 3(8), 529–536. https://www.ijert.org/research/utilization-of-waste-	plastic-	in-manufacturing-of-plastic-soil-bricks-IJERTV3IS080515.pdf

Madu, V. C., Onyelowe, K. C., & Olawale, O. P. (2024). Durability evaluation of lime–CCR–	PWG-stabilized expansive clay for foundation application. Geotechnical Research, 11(1), 	72–84.

Mahmmod, L. M. R., & Abbas, W. A. (2025). Potential impact of calcium carbide residue on the 	fresh and hardened behavior of eco-friendly cement-based composites. Cleaner Waste 	Systems, 100307.

Mitchell, J. K., & Soga, K. (2005). Fundamentals of soil behavior (3rd ed.). John Wiley & Sons.

Mohammadi Darestani, A., Arabani, M., Zanganeh Ranjbar, P., Payan, M., & Salimi, M. (2025). 	Strength enhancement of calcium carbide residue-stabilized clay with perlite powder and 	water treatment sludge. Scientific Reports, 15(1), 43701.

Muhmed, A. A., & Wanatowski, D. (2013). Effect of lime content on engineering properties of 	clay soil. Proceedings of the ICE – Ground Improvement, 166(4), 189–197.

Muntohar, A. S. (2019). Strength and microstructure of clay–fly-ash–plastic-waste stabilized soils.	 International Journal of Geotechnical Engineering, 13(5), 481–490.

Mechanistic lateritic soil study (2025). Mechanistic and comparative laboratory assessment of lime 	dosage and uniaxial geogrid on strength and durability of lateritic subgrade. Scientific 	Reports, 15. (PI reduced significantly with lime stabilization).

Neale, R. E., Barnes, P. W., Robson, T. M., Neale, P. J., Williamson, C. E., Zepp, R. G., ... & Zhu, 	M. (2021). Environmental effects of stratospheric ozone depletion, UV radiation, and 	interactions with climate change: UNEP Environmental Effects Assessment Panel, Update 	2020. Photochemical & Photobiological Sciences, 20(1), 1-67,

Nelson, J. D., & Miller, D. J. (1992). Expansive soils: Problems and practice in foundation and 	pavement engineering. John Wiley & Sons.

Nnadi, E. O. E., & Najjobyo, J. (2025). Financial and operational effects of cost estimation 	inaccuracy, material price volatility, and payment delays in Nigerian construction projects. 	Smart Construction and Sustainable Cities, 3(1), 29.

Ogunribido, T. H. T., & Abiola, B. (2015). Geotechnical properties of expansive soils in 	southwestern Nigeria. Journal of Earth Sciences and Geotechnical Engineering, 5(2), 77–	86.

Ojuri, O. O., Osagie, P. O., Oluyemi-Ayibiowu, B. D., Fadugba, O. G., Tanimola, M. O., Chauhan, 	V. B., & Jayejeje, O. O. (2022). Eco-friendly stabilization of highway lateritic soil with 	cow bone powder admixed lime and plastic granules reinforcement. Cleaner Waste 	Systems, 2, 100012.

Ola, S. A. (1974). Need for estimated cement requirements for stabilizing lateritic soils. Journal of 	the Transportation Engineering Division, 100(2), 379–388.

Onyelowe, K. C., Eberemu, A. O., & Van, D. T. (2020). Engineering behavior of clay stabilized 	with calcium-carbide residue and waste additives. Environmental Geotechnics, 7(5), 353–	367.

ONYELOWE, K. C., ONYIA, M. E., ONUKWUGHA, E. R., Nnadi, O. C., ONUOHA, I. C., & 	JALAL, F. E. (2020). Polynomial relationship of compaction properties of silicate-based 	RHA modified expansive soil for pavement subgrade purposes. Építőanyag: Journal of 	Silicate Based & Composite Materials, 72(6).

Onyelowe, K., Salahudeen, A. B., Eberemu, A., Ezugwu, C., Amhadi, T., Alaneme, G., & Sosa, 	F. (2019, November). Utilization of solid waste derivative materials in soft soils re-	engineering. In International Congress and Exhibition" Sustainable Civil Infrastructures” 	(pp. 49-57). Cham: Springer International Publishing.

Osinubi, K. J., Eberemu, A. O., & Amadi, A. A. (2019). Soil stabilization for road and building 	foundations: A Nigerian perspective. Nigerian Journal of Technology, 38(1), 21–32.

Piechowicz, K., Szymanek, S., Kowalski, J., & Lendo-Siwicka, M. (2024). Stabilization of loose 	soils as part of sustainable development of road infrastructure. Sustainability, 16(9), 3592.

Sandamali, D. M. T. U., & Sampath, K. H. S. M. (2022). Applicability of calcium carbide residue 	for soil stabilization: A systematic review and a meta-analysis (Conference paper). 	Department of Civil Engineering, Faculty of Engineering, University of Moratuwa. 	http://dl.lib.uom.lk/handle/123/20284.

Shinde, B., Sangale, A., Pranita, M., Sanagle, J., & Roham, C. (2024). Utilization of waste 	materials for soil stabilization: A comprehensive review. Progress in Engineering Science, 	1(2-3), 100009.

Singh, A., & Sugandhi, S. (2024). Soil stabilization using plastic waste and limestone. 	International Journal of Science, Engineering and Technology, 12(6). 	https://www.ijset.in/wp-content/uploads/IJSET_V12_issue6_881.pdf

Sorsa, A., Senadheera, S., & Birru, Y. (2020). Engineering characterization of subgrade soils of 	Jimma town, Ethiopia, for roadway design. Geosciences, 10(3), 94.

Tang, P., Javadi, A. A., & Vinai, R. (2025). Calcium carbide residue for clay stabilisation: 	mechanical and microstructural properties. Transportation Geotechnics, 51, 101543.

Transport Research Laboratory (TRL). (1993). Overseas Road Note 31: A guide to the structural 	design of bitumen-surfaced roads in tropical and sub-tropical countries. TRL, UK.

UNEP. (2019). Global status report for buildings and construction: Towards a zero-emission, 	efficient and resilient buildings and construction sector. United Nations Environment 	Programme.

UNEP. (2021). From pollution to solution: A global assessment of marine litter and plastic 	pollution. United Nations Environment Programme.

World Bank. (2022). Nigeria: Plastic waste and circular economy assessment report. World Bank 	Group.

Waleed, M., & Alshawmar, F. (2025). Enhancing mechanical properties of low plasticity soil 	through coal waste and silica fume stabilization. Scientific Reports, 15(1), 9990. 	https://doi.org/10.1038/s41598-025-94149-0

Zhang, S., Li, J., Li, G., Nie, Y., Qiang, L., Bai, B., & Ma, X. (2021). Life cycle assessment of 	acetylene production from calcium carbide and methane in China. Journal of Cleaner 	Production, 322, 129055. https://doi.org/10.1016/J.JCLEPRO.2021.129055

APPENDIX

SPECIFIC GRAVITY

| Trials | 1 | 2 |
| --- | --- | --- |
| Weight of empty bottle (g) | 28.42 | 27.28 |
| Weight of empty bottle + dry soil (g) | 56.34 | 56.32 |
| Weight of bottle + soil + water (g) | 93.58 | 93.23 |
| Weight of bottle + water (g) | 77.00 | 76.00 |
| Specific Gravity | 2.46 | 2.46 |
| Average Specific Gravity | 2.46 |  |

MECHANICAL SIEVE

| Sieve Sizes (mm) | Weight retained (g) | % Weight Retained | % Passing |
| --- | --- | --- | --- |
| 9.5 | 57.71 | 5.77 | 94.23 |
| 4.75 | 92.88 | 9.29 | 84.94 |
| 2.36 | 111.35 | 11.14 | 73.81 |
| 1.18 | 66.78 | 6.68 | 67.13 |
| 0.6 | 49.24 | 4.92 | 62.20 |
| 0.3 | 41.07 | 4.11 | 58.10 |
| 0.15 | 42.59 | 4.26 | 53.84 |
| 0.075 | 25.41 | 2.54 | 51.30 |

HYDROMETER

| Elapsed Time (min) | Actual Hydrometer Reading | Corrected Hydrometer Reading | Effective Depth L (cm) | D (x10-3) mm | K (10-3) | Percentage finer | Adjusted % finer |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 6.00 | 21.00 | 21.50 | 12.95 | 19.87 | 13.52 | 45.41 | 23.29 |
| 26.00 | 18.00 | 18.50 | 13.25 | 9.65 | 13.52 | 39.07 | 20.04 |
| 85.00 | 15.00 | 15.50 | 13.75 | 5.44 | 13.52 | 32.74 | 16.79 |
| 240.00 | 13.00 | 13.50 | 14.10 | 3.28 | 13.52 | 28.51 | 14.63 |
| 405.00 | 11.50 | 12.00 | 14.30 | 2.54 | 13.52 | 25.34 | 13.00 |
| 760.00 | 10.50 | 11.00 | 14.50 | 1.87 | 13.52 | 23.23 | 11.92 |
| 1065.00 | 10.00 | 10.50 | 14.60 | 1.58 | 13.52 | 22.18 | 11.38 |
| 1380.00 | 9.50 | 10.00 | 14.70 | 1.40 | 13.52 | 21.12 | 10.83 |

ATTERBERG LIMITS

| 0% |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 7.86% |
| Initial Penetration (mm) | 2.1 | 2.3 | 2.3 | 2.6 |  |  |  |
| Final Penetration (mm) | 11.5 | 22.2 | 25.1 | 30.5 |  |  |  |
| Actual Penetration (mm) | 9.4 | 19.9 | 22.8 | 27.9 | A | B |  |
| Can Weight (g) | 6.67 | 8.75 | 5.78 | 3.24 | 2.70 | 3.98 |  |
| Weight of Can + Wet Soil (g) | 22.60 | 30.47 | 27.17 | 24.40 | 14.19 | 16.38 |  |
| Weight of can + Dry Soil (g) | 17.67 | 22.69 | 19.28 | 15.90 | 11.49 | 13.40 |  |
| Moisture Contents (%) | 44.82 | 55.81 | 58.44 | 67.14 | 30.72 | 31.63 |  |
| Average Moisture Contents (%) |  |  |  |  | 31.18 |  |  |

| SOIL + 6% LIME |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 6.43% |
| Initial Penetration (mm) | 1.9 | 2.4 | 2.4 | 3.9 |  |  |  |
| Final Penetration (mm) | 16.0 | 22.9 | 27.5 | 32.9 |  |  |  |
| Actual Penetration (mm) | 14.1 | 20.5 | 25.1 | 29.0 | A | B |  |
| Can Weight (g) | 6.68 | 5.81 | 13.01 | 7.57 | 4.82 | 3.88 |  |
| Weight of Can + Wet Soil (g) | 23.34 | 19.91 | 40.65 | 23.87 | 19.15 | 17.58 |  |
| Weight of can + Dry Soil (g) | 17.66 | 14.65 | 29.57 | 16.98 | 14.42 | 13.13 |  |
| Moisture Contents (%) | 51.73 | 59.50 | 66.91 | 73.22 | 49.27 | 48.11 |  |
| Average Moisture Contents (%) |  |  |  |  | 48.69 |  |  |

| SOIL+6%LIME+1%CCR |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 7.97% |
| Initial Penetration (mm) | 5.0 | 5.5 | 5.5 | 6.0 |  |  |  |
| Final Penetration (mm) | 19.3 | 21.5 | 30.3 | 37.5 |  |  |  |
| Actual Penetration (mm) | 14.3 | 16.0 | 24.8 | 31.5 | A | B |  |
| Can Weight (g) | 3.13 | 3.55 | 4.72 | 2.58 | 3.74 | 10.91 |  |
| Weight of Can + Wet Soil (g) | 7.98 | 11.99 | 16.48 | 14.19 | 8.65 | 16.31 |  |
| Weight of can + Dry Soil (g) | 5.97 | 8.40 | 11.20 | 8.74 | 7.02 | 14.53 |  |
| Moisture Contents (%) | 70.77 | 74.02 | 81.48 | 88.47 | 49.70 | 49.17 |  |
| Average Moisture Contents (%) |  |  |  |  | 49.43 |  |  |

| SOIL+6%LIME+1%CCR+0.5%PW |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 7.86% |
| Initial Penetration (mm) | 4.5 | 6.1 | 5.5 | 5.3 |  |  |  |
| Final Penetration (mm) | 16.5 | 23.5 | 34.0 | 38.6 |  |  |  |
| Actual Penetration (mm) | 12.0 | 17.4 | 28.5 | 33.3 | A | B |  |
| Can Weight (g) | 4.62 | 5.40 | 7.23 | 10.80 | 5.73 | 11.72 |  |
| Weight of Can + Wet Soil (g) | 15.22 | 16.58 | 20.97 | 21.11 | 13.66 | 17.32 |  |
| Weight of can + Dry Soil (g) | 10.81 | 11.72 | 14.75 | 16.32 | 10.97 | 15.41 |  |
| Moisture Contents (%) | 71.24 | 76.90 | 82.71 | 86.78 | 51.34 | 51.76 |  |
| Average Moisture Contents (%) |  |  |  |  | 51.55 |  |  |

| SOIL+6%LIME+1%CCR+1%PW |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 7.86% |
| Initial Penetration (mm) | 6.0 | 6.0 | 6.5 | 6.2 |  |  |  |
| Final Penetration (mm) | 21.0 | 23.3 | 28.9 | 34.0 |  |  |  |
| Actual Penetration (mm) | 15.0 | 17.3 | 22.4 | 27.8 | A | B |  |
| Can Weight (g) | 8.38 | 3.83 | 5.05 | 2.65 | 3.65 | 3.51 |  |
| Weight of Can + Wet Soil (g) | 15.85 | 10.14 | 15.86 | 11.57 | 7.80 | 7.42 |  |
| Weight of can + Dry Soil (g) | 12.74 | 7.45 | 11.03 | 7.40 | 6.37 | 6.07 |  |
| Moisture Contents (%) | 71.33 | 74.31 | 80.77 | 87.79 | 52.57 | 52.73 |  |
| Average Moisture Contents (%) |  |  |  |  | 52.65 |  |  |

| SOIL+6%LIME+1%CCR+1.5%PW |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 7.25% |
| Initial Penetration (mm) | 6.9 | 7.1 | 6.7 | 7.1 |  |  |  |
| Final Penetration (mm) | 20.0 | 24.9 | 34.3 | 39.0 |  |  |  |
| Actual Penetration (mm) | 13.1 | 17.8 | 27.6 | 31.9 | A | B |  |
| Can Weight (g) | 7.07 | 6.75 | 7.58 | 4.64 | 15.05 | 11.28 |  |
| Weight of Can + Wet Soil (g) | 19.51 | 23.01 | 26.97 | 24.60 | 30.50 | 28.54 |  |
| Weight of can + Dry Soil (g) | 14.22 | 15.74 | 17.97 | 15.00 | 25.16 | 22.56 |  |
| Moisture Contents (%) | 73.99 | 80.87 | 86.62 | 92.66 | 52.82 | 53.01 |  |
| Average Moisture Contents (%) |  |  |  |  | 52.92 |  |  |

| SOIL+6%LIME+1%CCR+2%PW |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 7.14% |
| Initial Penetration (mm) | 6.1 | 6.4 | 6.1 | 6.0 |  |  |  |
| Final Penetration (mm) | 21.0 | 26.5 | 28.7 | 33.3 |  |  |  |
| Actual Penetration (mm) | 14.9 | 20.1 | 22.6 | 27.3 | A | B |  |
| Can Weight (g) | 15.17 | 2.86 | 2.47 | 3.95 | 7.87 | 3.16 |  |
| Weight of Can + Wet Soil (g) | 26.33 | 11.22 | 12.01 | 21.10 | 14.39 | 8.36 |  |
| Weight of can + Dry Soil (g) | 21.52 | 7.43 | 7.58 | 12.85 | 12.13 | 6.67 |  |
| Moisture Contents (%) | 75.75 | 82.93 | 86.69 | 92.70 | 53.05 | 48.15 |  |
| Average Moisture Contents (%) |  |  |  |  | 50.60 |  |  |

| SOIL+6%LIME+2%CCR |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 7.86% |
| Initial Penetration (mm) | 5.8 | 6.3 | 4.9 | 5.5 |  |  |  |
| Final Penetration (mm) | 18.0 | 23.3 | 32.5 | 35.0 |  |  |  |
| Actual Penetration (mm) | 12.2 | 17.0 | 27.6 | 29.5 | A | B |  |
| Can Weight (g) | 3.17 | 3.40 | 10.33 | 2.62 | 8.85 | 4.08 |  |
| Weight of Can + Wet Soil (g) | 11.52 | 15.05 | 20.33 | 23.52 | 13.68 | 9.35 |  |
| Weight of can + Dry Soil (g) | 8.07 | 10.08 | 15.82 | 14.00 | 12.12 | 7.63 |  |
| Moisture Contents (%) | 70.41 | 74.40 | 82.15 | 83.66 | 47.71 | 48.45 |  |
| Average Moisture Contents (%) |  |  |  |  | 48.08 |  |  |

| SOIL+6%LIME+2%CCR+0.5%PW |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 7.14% |
| Initial Penetration (mm) | 6.3 | 6.9 | 7.1 | 7.5 |  |  |  |
| Final Penetration (mm) | 19.1 | 26.0 | 31.0 | 38.0 |  |  |  |
| Actual Penetration (mm) | 12.8 | 19.1 | 23.9 | 30.5 | A | B |  |
| Can Weight (g) | 2.86 | 3.68 | 1.67 | 3.64 | 2.73 | 3.68 |  |
| Weight of Can + Wet Soil (g) | 13.95 | 14.16 | 11.75 | 14.05 | 7.97 | 8.34 |  |
| Weight of can + Dry Soil (g) | 9.26 | 9.56 | 7.18 | 9.15 | 6.14 | 6.71 |  |
| Moisture Contents (%) | 73.28 | 78.23 | 82.94 | 88.93 | 53.67 | 53.80 |  |
| Average Moisture Contents (%) |  |  |  |  | 53.73 |  |  |

| SOIL+6%LIME+2%CCR+1%PW |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |  |
| Trials | 1 | 2 | 3 | 4 |  |  | 8.63% |  |
| Initial Penetration (mm) | 5.7 | 6.1 | 5.8 | 7.0 |  |  |  |  |
| Final Penetration (mm) | 17.5 | 23.0 | 31.1 | 34.2 |  |  |  |  |
| Actual Penetration (mm) | 11.8 | 16.9 | 25.3 | 27.2 | A | B |  |  |
| Can Weight (g) | 2.73 | 1.56 | 9.31 | 7.68 | 2.36 | 3.35 |  |  |
| Weight of Can + Wet Soil (g) | 16.91 | 5.96 | 31.68 | 20.79 | 6.32 | 9.57 |  |  |
| Weight of can + Dry Soil (g) | 11.21 | 4.09 | 21.60 | 14.72 | 4.94 | 7.40 |  |  |
| Moisture Contents (%) | 67.22 | 73.91 | 82.02 | 86.22 | 53.49 | 53.58 |  |  |
| Average Moisture Contents (%) |  |  |  |  | 53.53 |  |  |  |

| SOIL+6%LIME+2%CCR+1.5%PW |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 7.97% |
| Initial Penetration (mm) | 6.6 | 6.2 | 6.9 | 6.7 |  |  |  |
| Final Penetration (mm) | 19.9 | 23.4 | 27.8 | 32.0 |  |  |  |
| Actual Penetration (mm) | 13.3 | 17.2 | 20.9 | 25.3 | A | B |  |
| Can Weight (g) | 2.65 | 5.60 | 3.79 | 7.65 | 6.36 | 8.87 |  |
| Weight of Can + Wet Soil (g) | 14.71 | 15.69 | 13.05 | 16.46 | 11.08 | 12.71 |  |
| Weight of can + Dry Soil (g) | 9.89 | 11.32 | 8.87 | 12.24 | 9.45 | 11.37 |  |
| Moisture Contents (%) | 66.57 | 76.40 | 82.28 | 91.94 | 52.75 | 53.60 |  |
| Average Moisture Contents (%) |  |  |  |  | 53.18 |  |  |

| SOIL+6%LIME+2%CCR+2%PW |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | LIQUID LIMIT |  |  |  | PLASTIC LIMIT |  | LS |
| Trials | 1 | 2 | 3 | 4 |  |  | 6.98% |
| Initial Penetration (mm) | 7.4 | 5.4 | 5.9 | 6.0 |  |  |  |
| Final Penetration (mm) | 21.5 | 23.5 | 29.5 | 36.2 |  |  |  |
| Actual Penetration (mm) | 14.1 | 18.1 | 23.6 | 30.2 | A | B |  |
| Can Weight (g) | 3.59 | 7.97 | 4.11 | 6.99 | 7.35 | 7.18 |  |
| Weight of Can + Wet Soil (g) | 15.02 | 18.67 | 15.72 | 19.22 | 13.01 | 14.24 |  |
| Weight of can + Dry Soil (g) | 10.00 | 13.85 | 10.33 | 13.42 | 11.05 | 11.80 |  |
| Moisture Contents (%) | 78.32 | 81.97 | 86.66 | 90.20 | 52.97 | 52.81 |  |
| Average Moisture Contents (%) |  |  |  |  | 52.89 |  |  |

COMPACTION

| 0% |  |  |  |  |
| --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 |
| Weight of Mould (Kg) | 2.50 | 2.50 | 2.50 | 2.50 |
| Mould + Wet Soil (Kg) | 4.30 | 4.45 | 4.55 | 4.50 |
| Weight of Wet Soil (Kg) | 1.80 | 1.95 | 2.05 | 2.00 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1800 | 1950 | 2050 | 2000 |
| Weight of empty can (g) | 10.34 | 4.87 | 12.02 | 4.97 |
| Can + wet sample (g) | 31.09 | 18.79 | 29.94 | 17.43 |
| Can + dry sample (g) | 29.36 | 17.25 | 27.58 | 15.58 |
| Moisture Content (%) | 9.10 | 12.44 | 15.17 | 17.44 |
| Dry Density (Kg/m3) | 1650 | 1734 | 1780 | 1703 |

| SOIL+6% LIME |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 | 5 |
| Weight of Mould (Kg) | 2.50 | 2.50 | 2.50 | 2.50 | 2.50 |
| Mould + Wet Soil (Kg) | 4.40 | 4.50 | 4.60 | 4.70 | 4.60 |
| Weight of Wet Soil (Kg) | 1.90 | 2.00 | 2.10 | 2.20 | 2.10 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1900 | 2000 | 2100 | 2200 | 2100 |
| Weight of empty can (g) | 4.78 | 10.43 | 5.21 | 10.54 | 6.43 |
| Can + wet sample (g) | 22.01 | 36.02 | 26.12 | 29.45 | 21.06 |
| Can + dry sample (g) | 20.23 | 32.81 | 23.00 | 26.16 | 18.32 |
| Moisture Content (%) | 11.52 | 14.34 | 17.54 | 21.06 | 23.04 |
| Dry Density (Kg/m3) | 1704 | 1749 | 1787 | 1817 | 1707 |

| SOIL+6%LIME+1%CCR |  |  |  |  |
| --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 |
| Weight of Mould (Kg) | 2.50 | 2.50 | 2.50 | 2.50 |
| Mould + Wet Soil (Kg) | 4.40 | 4.50 | 4.60 | 4.50 |
| Weight of Wet Soil (Kg) | 1.90 | 2.00 | 2.10 | 2.00 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1900 | 2000 | 2100 | 2000 |
| Weight of empty can (g) | 3.29 | 2.38 | 3.13 | 3.62 |
| Can + wet sample (g) | 10.27 | 11.42 | 17.16 | 16.85 |
| Can + dry sample (g) | 9.32 | 10.08 | 14.88 | 14.52 |
| Moisture Content (%) | 15.75 | 17.40 | 19.40 | 21.38 |
| Dry Density (Kg/m3) | 1641 | 1704 | 1759 | 1648 |

| SOIL+6%LIME+2%CCR |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 | 5 |
| Weight of Mould (Kg) | 2.50 | 2.50 | 2.50 | 2.50 | 2.50 |
| Mould + Wet Soil (Kg) | 4.30 | 4.45 | 4.55 | 4.60 | 4.50 |
| Weight of Wet Soil (Kg) | 1.80 | 1.95 | 2.05 | 2.10 | 2.00 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1800 | 1950 | 2050 | 2100 | 2000 |
| Weight of empty can (g) | 8.67 | 1.78 | 3.04 | 3.72 | 3.60 |
| Can + wet sample (g) | 31.18 | 10.00 | 13.86 | 19.05 | 31.46 |
| Can + dry sample (g) | 28.65 | 8.89 | 12.20 | 16.41 | 26.29 |
| Moisture Content (%) | 12.66 | 15.61 | 18.12 | 20.80 | 22.79 |
| Dry Density (Kg/m3) | 1598 | 1687 | 1735 | 1738 | 1629 |

| SOIL+6%LIME+1%CCR+0.5%PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 |
| Weight of Mould (Kg) | 2.50 | 2.50 | 2.50 | 2.50 |
| Mould + Wet Soil (Kg) | 4.40 | 4.55 | 4.65 | 4.55 |
| Weight of Wet Soil (Kg) | 1.90 | 2.05 | 2.15 | 2.05 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1900 | 2050 | 2150 | 2050 |
| Weight of empty can (g) | 2.56 | 9.40 | 3.40 | 8.08 |
| Can + wet sample (g) | 28.36 | 38.73 | 18.19 | 40.00 |
| Can + dry sample (g) | 24.91 | 34.41 | 15.78 | 34.36 |
| Moisture Content (%) | 15.44 | 17.27 | 19.47 | 21.46 |
| Dry Density (Kg/m3) | 1646 | 1748 | 1800 | 1688 |

| SOIL+6%LIME+1%CCR+1%PW |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 | 5 |
| Weight of Mould (Kg) | 3.40 | 3.40 | 3.40 | 3.40 | 3.40 |
| Mould + Wet Soil (Kg) | 5.20 | 5.30 | 5.40 | 5.50 | 5.40 |
| Weight of Wet Soil (Kg) | 1.80 | 1.90 | 2.00 | 2.10 | 2.00 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1800 | 1900 | 2000 | 2100 | 2000 |
| Weight of empty can (g) | 1.90 | 2.16 | 5.10 | 7.74 | 3.91 |
| Can + wet sample (g) | 15.51 | 15.37 | 18.68 | 23.42 | 22.40 |
| Can + dry sample (g) | 14.21 | 13.89 | 16.89 | 20.92 | 19.11 |
| Moisture Content (%) | 10.56 | 12.62 | 15.18 | 18.97 | 21.64 |
| Dry Density (Kg/m3) | 1628 | 1687 | 1736 | 1765 | 1644 |

| SOIL+6%LIME+1%CCR+1.5%PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 |
| Weight of Mould (Kg) | 2.50 | 2.50 | 2.50 | 2.50 |
| Mould + Wet Soil (Kg) | 4.30 | 4.40 | 4.50 | 4.45 |
| Weight of Wet Soil (Kg) | 1.80 | 1.90 | 2.00 | 1.95 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1800 | 1900 | 2000 | 1950 |
| Weight of empty can (g) | 10.91 | 8.87 | 7.92 | 6.40 |
| Can + wet sample (g) | 52.45 | 31.22 | 37.24 | 32.20 |
| Can + dry sample (g) | 48.12 | 28.47 | 33.13 | 28.12 |
| Moisture Content (%) | 11.64 | 14.03 | 16.30 | 18.78 |
| Dry Density (Kg/m3) | 1612 | 1666 | 1720 | 1642 |

| SOIL+6%LIME+1%CCR+2%PW |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 | 5 |
| Weight of Mould (Kg) | 3.10 | 3.10 | 3.10 | 3.10 | 3.10 |
| Mould + Wet Soil (Kg) | 4.90 | 5.00 | 5.10 | 5.20 | 5.10 |
| Weight of Wet Soil (Kg) | 1.80 | 1.90 | 2.00 | 2.10 | 2.00 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1800 | 1900 | 2000 | 2100 | 2000 |
| Weight of empty can (g) | 12.17 | 4.09 | 6.36 | 5.79 | 8.27 |
| Can + wet sample (g) | 46.51 | 21.19 | 25.74 | 22.70 | 27.60 |
| Can + dry sample (g) | 42.78 | 18.95 | 22.76 | 19.61 | 23.76 |
| Moisture Content (%) | 12.19 | 15.07 | 18.17 | 22.36 | 24.79 |
| Dry Density (Kg/m3) | 1604 | 1651 | 1692 | 1716 | 1603 |

| SOIL+6%LIME+2%CCR+0.5%PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 |
| Weight of Mould (Kg) | 3.40 | 3.40 | 3.40 | 3.40 |
| Mould + Wet Soil (Kg) | 5.20 | 5.30 | 5.40 | 5.35 |
| Weight of Wet Soil (Kg) | 1.80 | 1.90 | 2.00 | 1.95 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1800 | 1900 | 2000 | 1950 |
| Weight of empty can (g) | 5.24 | 3.20 | 3.01 | 4.26 |
| Can + wet sample (g) | 22.94 | 20.67 | 25.30 | 29.45 |
| Can + dry sample (g) | 20.83 | 18.32 | 21.97 | 25.30 |
| Moisture Content (%) | 13.53 | 15.54 | 17.56 | 19.72 |
| Dry Density (Kg/m3) | 1585 | 1644 | 1701 | 1629 |

| SOIL+6%LIME+2%CCR+1%PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 |
| Weight of Mould (Kg) | 2.50 | 2.50 | 2.50 | 2.50 |
| Mould + Wet Soil (Kg) | 4.25 | 4.35 | 4.50 | 4.40 |
| Weight of Wet Soil (Kg) | 1.75 | 1.85 | 2.00 | 1.90 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1750 | 1850 | 2000 | 1900 |
| Weight of empty can (g) | 6.97 | 6.74 | 5.41 | 2.94 |
| Can + wet sample (g) | 31.68 | 29.44 | 26.45 | 30.32 |
| Can + dry sample (g) | 29.19 | 26.76 | 23.54 | 26.00 |
| Moisture Content (%) | 11.21 | 13.39 | 16.05 | 18.73 |
| Dry Density (Kg/m3) | 1574 | 1632 | 1723 | 1600 |

| SOIL+6%LIME+2%CCR+1.5%PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 |
| Weight of Mould (Kg) | 3.10 | 3.10 | 3.10 | 3.10 |
| Mould + Wet Soil (Kg) | 4.90 | 5.00 | 5.10 | 5.05 |
| Weight of Wet Soil (Kg) | 1.80 | 1.90 | 2.00 | 1.95 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1800 | 1900 | 2000 | 1950 |
| Weight of empty can (g) | 2.07 | 7.04 | 6.70 | 5.01 |
| Can + wet sample (g) | 14.29 | 24.19 | 26.46 | 23.42 |
| Can + dry sample (g) | 13.02 | 22.07 | 23.62 | 20.38 |
| Moisture Content (%) | 11.60 | 14.11 | 16.78 | 19.78 |
| Dry Density (Kg/m3) | 1613 | 1665 | 1713 | 1628 |

| SOIL+6%LIME+2%CCR+2%PW |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Trial | 1 | 2 | 3 | 4 | 5 |
| Weight of Mould (Kg) | 3.40 | 3.40 | 3.40 | 3.40 | 3.40 |
| Mould + Wet Soil (Kg) | 5.20 | 5.30 | 5.40 | 5.45 | 5.40 |
| Weight of Wet Soil (Kg) | 1.80 | 1.90 | 2.00 | 2.05 | 2.00 |
| Volume of Mould (m3) | 0.001 | 0.001 | 0.001 | 0.001 | 0.001 |
| Bulk Density (Kg/m3) | 1800 | 1900 | 2000 | 2050 | 2000 |
| Weight of empty can (g) | 3.06 | 2.88 | 2.59 | 6.36 | 1.91 |
| Can + wet sample (g) | 12.25 | 17.69 | 10.64 | 17.69 | 13.53 |
| Can + dry sample (g) | 11.06 | 15.47 | 9.28 | 15.60 | 11.21 |
| Moisture Content (%) | 14.88 | 17.63 | 20.33 | 22.62 | 24.95 |
| Dry Density (Kg/m3) | 1567 | 1615 | 1662 | 1672 | 1601 |

UCS

| NATURAL SOIL |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.006024 | 0.001134 | 0.001141 | 12 | 0.024 | 21.04 | 15 | 0.03 | 26.30 | 15 | 0.03 | 26.30 |
| 1.00 | 0.012048 | 0.001134 | 0.001148 | 29 | 0.058 | 50.53 | 27 | 0.054 | 47.05 | 29 | 0.058 | 50.53 |
| 1.50 | 0.018072 | 0.001134 | 0.001155 | 38 | 0.076 | 65.81 | 42 | 0.084 | 72.74 | 44 | 0.088 | 76.20 |
| 2.00 | 0.024096 | 0.001134 | 0.001162 | 52 | 0.104 | 89.50 | 56 | 0.112 | 96.39 | 61 | 0.122 | 104.99 |
| 2.50 | 0.030120 | 0.001134 | 0.001169 | 67 | 0.134 | 114.61 | 65 | 0.13 | 111.19 | 69 | 0.138 | 118.03 |
| 3.00 | 0.036145 | 0.001134 | 0.001177 | 82 | 0.164 | 139.39 | 78 | 0.156 | 132.59 | 82 | 0.164 | 139.39 |
| 3.50 | 0.042169 | 0.001134 | 0.001184 | 88 | 0.176 | 148.66 | 86 | 0.172 | 145.28 | 88 | 0.176 | 148.66 |
| 4.00 | 0.048193 | 0.001134 | 0.001191 | 84 | 0.168 | 141.01 | 75 | 0.15 | 125.90 | 81 | 0.162 | 135.97 |
| UCS (kN/m2) |  |  |  | 147.53 |  |  |  |  |  |  |  |  |

| SOIL + 6%L |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.005814 | 0.001134 | 0.001141 | 15 | 0.03 | 26.30 | 18 | 0.036 | 31.56 | 21 | 0.042 | 36.82 |
| 1.00 | 0.011628 | 0.001134 | 0.001147 | 32 | 0.064 | 55.78 | 37 | 0.074 | 64.50 | 45 | 0.09 | 78.44 |
| 1.50 | 0.017442 | 0.001134 | 0.001154 | 49 | 0.098 | 84.91 | 56 | 0.112 | 97.04 | 53 | 0.106 | 91.84 |
| 2.00 | 0.023256 | 0.001134 | 0.001161 | 66 | 0.132 | 113.70 | 72 | 0.144 | 124.03 | 68 | 0.136 | 117.14 |
| 2.50 | 0.029070 | 0.001134 | 0.001168 | 82 | 0.164 | 140.42 | 87 | 0.174 | 148.98 | 87 | 0.174 | 148.98 |
| 3.00 | 0.034884 | 0.001134 | 0.001175 | 104 | 0.208 | 177.02 | 105 | 0.21 | 178.73 | 102 | 0.204 | 173.62 |
| 3.50 | 0.040698 | 0.001134 | 0.001182 | 96 | 0.192 | 162.42 | 89 | 0.178 | 150.58 | 95 | 0.19 | 160.73 |
| UCS (kN/m2) |  |  |  | 176.46 |  |  |  |  |  |  |  |  |

| SOIL + 6%L + 1%CCR |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.25 | 0.002907 | 0.001134 | 0.001137 | 17 | 0.034 | 29.90 | 21 | 0.042 | 36.93 | 19 | 0.038 | 33.41 |
| 0.50 | 0.005814 | 0.001134 | 0.001141 | 39 | 0.078 | 68.38 | 36 | 0.072 | 63.12 | 34 | 0.068 | 59.62 |
| 0.75 | 0.008721 | 0.001134 | 0.001144 | 53 | 0.106 | 92.66 | 48 | 0.096 | 83.92 | 56 | 0.112 | 97.90 |
| 1.00 | 0.011628 | 0.001134 | 0.001147 | 68 | 0.136 | 118.53 | 63 | 0.126 | 109.82 | 71 | 0.142 | 123.76 |
| 1.25 | 0.014535 | 0.001134 | 0.001151 | 81 | 0.162 | 140.78 | 75 | 0.15 | 130.35 | 82 | 0.164 | 142.52 |
| 1.50 | 0.017442 | 0.001134 | 0.001154 | 96 | 0.192 | 166.36 | 89 | 0.178 | 154.23 | 97 | 0.194 | 168.09 |
| 1.75 | 0.020349 | 0.001134 | 0.001158 | 105 | 0.21 | 181.42 | 95 | 0.19 | 164.14 | 109 | 0.218 | 188.33 |
| 2.00 | 0.023256 | 0.001134 | 0.001161 | 113 | 0.226 | 194.66 | 109 | 0.218 | 187.77 | 114 | 0.228 | 196.38 |
| 2.25 | 0.026163 | 0.001134 | 0.001164 | 104 | 0.208 | 178.62 | 115 | 0.23 | 197.52 | 101 | 0.202 | 173.47 |
| 2.50 | 0.029070 | 0.001134 | 0.001168 |  |  |  | 104 | 0.208 | 178.09 |  |  |  |
| UCS (kN/m2) |  |  |  | 196.19 |  |  |  |  |  |  |  |  |

| SOIL + 6%L + 2%CCR |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.005556 | 0.001134 | 0.001140 | 15 | 0.03 | 26.31 | 18 | 0.036 | 31.57 | 16 | 0.032 | 28.06 |
| 1.00 | 0.011111 | 0.001134 | 0.001147 | 37 | 0.074 | 64.53 | 29 | 0.058 | 50.58 | 29 | 0.058 | 50.58 |
| 1.50 | 0.016667 | 0.001134 | 0.001153 | 42 | 0.084 | 72.84 | 43 | 0.086 | 74.57 | 45 | 0.09 | 78.04 |
| 2.00 | 0.022222 | 0.001134 | 0.001160 | 57 | 0.114 | 98.30 | 65 | 0.13 | 112.09 | 60 | 0.12 | 103.47 |
| 2.50 | 0.027778 | 0.001134 | 0.001166 | 72 | 0.144 | 123.46 | 82 | 0.164 | 140.60 | 74 | 0.148 | 126.89 |
| 3.00 | 0.033333 | 0.001134 | 0.001173 | 89 | 0.178 | 151.73 | 94 | 0.188 | 160.26 | 87 | 0.174 | 148.32 |
| 3.50 | 0.038889 | 0.001134 | 0.001180 | 102 | 0.204 | 172.90 | 105 | 0.21 | 177.98 | 95 | 0.19 | 161.03 |
| 4.00 | 0.044444 | 0.001134 | 0.001187 | 114 | 0.228 | 192.12 | 113 | 0.226 | 190.44 | 111 | 0.222 | 187.07 |
| 4.50 | 0.050000 | 0.001134 | 0.001194 | 126 | 0.252 | 211.11 | 119 | 0.238 | 199.38 | 124 | 0.248 | 207.76 |
| 5.00 | 0.055556 | 0.001134 | 0.001201 | 118 | 0.236 | 196.55 | 107 | 0.214 | 178.23 | 118 | 0.236 | 196.55 |
| UCS (kN/m2) |  |  |  | 206.08 |  |  |  |  |  |  |  |  |

| SOIL + 6%L + 1%CCR + 0.5PW |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.005556 | 0.001134 | 0.001140 | 23 | 0.046 | 40.34 | 25 | 0.05 | 43.85 | 21 | 0.042 | 36.83 |
| 1.00 | 0.011111 | 0.001134 | 0.001147 | 45 | 0.09 | 78.48 | 43 | 0.086 | 75.00 | 48 | 0.096 | 83.72 |
| 1.50 | 0.016667 | 0.001134 | 0.001153 | 62 | 0.124 | 107.52 | 67 | 0.134 | 116.20 | 75 | 0.15 | 130.07 |
| 2.00 | 0.022222 | 0.001134 | 0.001160 | 81 | 0.162 | 139.68 | 89 | 0.178 | 153.48 | 89 | 0.178 | 153.48 |
| 2.50 | 0.027778 | 0.001134 | 0.001166 | 96 | 0.192 | 164.61 | 108 | 0.216 | 185.19 | 107 | 0.214 | 183.47 |
| 3.00 | 0.033333 | 0.001134 | 0.001173 | 107 | 0.214 | 182.42 | 111 | 0.222 | 189.24 | 96 | 0.192 | 163.67 |
| 3.50 | 0.038889 | 0.001134 | 0.001180 | 101 | 0.202 | 171.20 | 102 | 0.204 | 172.90 |  |  |  |
| UCS (kN/m2) |  |  |  | 185.04 |  |  |  |  |  |  |  |  |

| SOIL + 6%L + 1%CCR + 1.0PW |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.005556 | 0.001134 | 0.001140 | 20 | 0.04 | 35.08 | 40 | 0.08 | 70.15 | 27 | 0.054 | 47.35 |
| 1.00 | 0.011111 | 0.001134 | 0.001147 | 30 | 0.06 | 52.32 | 45 | 0.09 | 78.48 | 45 | 0.09 | 78.48 |
| 1.50 | 0.016667 | 0.001134 | 0.001153 | 45 | 0.09 | 78.04 | 55 | 0.11 | 95.39 | 68 | 0.136 | 117.93 |
| 2.00 | 0.022222 | 0.001134 | 0.001160 | 55 | 0.11 | 94.85 | 65 | 0.13 | 112.09 | 82 | 0.164 | 141.41 |
| 2.50 | 0.027778 | 0.001134 | 0.001166 | 65 | 0.13 | 111.45 | 75 | 0.15 | 128.60 | 95 | 0.19 | 162.89 |
| 3.00 | 0.033333 | 0.001134 | 0.001173 | 75 | 0.15 | 127.87 | 85 | 0.17 | 144.91 | 102 | 0.204 | 173.90 |
| 3.50 | 0.038889 | 0.001134 | 0.001180 | 90 | 0.18 | 152.56 | 95 | 0.19 | 161.03 | 108 | 0.216 | 183.07 |
| 4.00 | 0.044444 | 0.001134 | 0.001187 | 100 | 0.2 | 168.53 | 105 | 0.21 | 176.95 | 97 | 0.194 | 163.47 |
| 4.50 | 0.050000 | 0.001134 | 0.001194 | 105 | 0.21 | 175.93 | 107 | 0.214 | 179.28 |  |  |  |
| 5.00 | 0.055556 | 0.001134 | 0.001201 | 110 | 0.22 | 183.23 | 110 | 0.22 | 183.23 |  |  |  |
| 5.50 | 0.061111 | 0.001134 | 0.001208 | 97 | 0.194 | 160.62 | 95 | 0.19 | 157.31 |  |  |  |
| UCS (kN/m2) |  |  |  | 183.17 |  |  |  |  |  |  |  |  |

| SOIL + 6%L + 1%CCR + 1.5PW |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.005882 | 0.001134 | 0.001141 | 27 | 0.054 | 47.34 | 31 | 0.062 | 54.35 | 27 | 0.054 | 47.34 |
| 1.00 | 0.011765 | 0.001134 | 0.001148 | 43 | 0.086 | 74.95 | 48 | 0.096 | 83.66 | 43 | 0.086 | 74.95 |
| 1.50 | 0.017647 | 0.001134 | 0.001154 | 60 | 0.12 | 103.95 | 64 | 0.128 | 110.88 | 56 | 0.112 | 97.02 |
| 2.00 | 0.023529 | 0.001134 | 0.001161 | 68 | 0.136 | 117.11 | 72 | 0.144 | 124.00 | 71 | 0.142 | 122.27 |
| 2.50 | 0.029412 | 0.001134 | 0.001168 | 75 | 0.15 | 128.38 | 79 | 0.158 | 135.23 | 85 | 0.17 | 145.50 |
| 3.00 | 0.035294 | 0.001134 | 0.001175 | 84 | 0.168 | 142.92 | 87 | 0.174 | 148.02 | 96 | 0.192 | 163.34 |
| 3.50 | 0.041176 | 0.001134 | 0.001183 | 89 | 0.178 | 150.50 | 93 | 0.186 | 157.27 | 103 | 0.206 | 174.18 |
| 4.00 | 0.047059 | 0.001134 | 0.001190 | 98 | 0.196 | 164.71 | 99 | 0.198 | 166.39 | 92 | 0.184 | 154.62 |
| 4.50 | 0.052941 | 0.001134 | 0.001197 | 86 | 0.172 | 143.65 | 102 | 0.204 | 170.37 |  |  |  |
| 5.00 | 0.058824 | 0.001134 | 0.001205 |  |  |  | 95 | 0.19 | 157.69 |  |  |  |
| UCS (kN/m2) |  |  |  | 169.75 |  |  |  |  |  |  |  |  |

| SOIL + 6%L + 1%CCR + 2.0PW |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.005882 | 0.001134 | 0.001141 | 32 | 0.064 | 56.11 | 28 | 0.056 | 49.09 | 29 | 0.058 | 50.85 |
| 1.00 | 0.011765 | 0.001134 | 0.001148 | 54 | 0.108 | 94.12 | 43 | 0.086 | 74.95 | 51 | 0.102 | 88.89 |
| 1.50 | 0.017647 | 0.001134 | 0.001154 | 67 | 0.134 | 116.08 | 59 | 0.118 | 102.22 | 69 | 0.138 | 119.55 |
| 2.00 | 0.023529 | 0.001134 | 0.001161 | 78 | 0.156 | 134.33 | 71 | 0.142 | 122.27 | 77 | 0.154 | 132.61 |
| 2.50 | 0.029412 | 0.001134 | 0.001168 | 89 | 0.178 | 152.35 | 86 | 0.172 | 147.21 | 85 | 0.17 | 145.50 |
| 3.00 | 0.035294 | 0.001134 | 0.001175 | 93 | 0.186 | 158.23 | 95 | 0.19 | 161.64 | 92 | 0.184 | 156.53 |
| 3.50 | 0.041176 | 0.001134 | 0.001183 | 88 | 0.176 | 148.81 | 87 | 0.174 | 147.12 | 95 | 0.19 | 160.65 |
| 4.00 | 0.047059 | 0.001134 | 0.001190 |  |  |  |  |  |  | 87 | 0.174 | 146.22 |
| UCS (kN/m2) |  |  |  | 160.17 |  |  |  |  |  |  |  |  |

| SOIL + 6%L + 2%CCR + 0.5PW |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.005556 | 0.001134 | 0.001140 | 27 | 0.054 | 47.35 | 32 | 0.064 | 56.12 | 31 | 0.062 | 54.37 |
| 1.00 | 0.011111 | 0.001134 | 0.001147 | 53 | 0.106 | 92.44 | 56 | 0.112 | 97.67 | 56 | 0.112 | 97.67 |
| 1.50 | 0.016667 | 0.001134 | 0.001153 | 87 | 0.174 | 150.88 | 87 | 0.174 | 150.88 | 78 | 0.156 | 135.27 |
| 2.00 | 0.022222 | 0.001134 | 0.001160 | 102 | 0.204 | 175.90 | 98 | 0.196 | 169.00 | 91 | 0.182 | 156.93 |
| 2.50 | 0.027778 | 0.001134 | 0.001166 | 116 | 0.232 | 198.90 | 113 | 0.226 | 193.76 | 109 | 0.218 | 186.90 |
| 3.00 | 0.033333 | 0.001134 | 0.001173 | 127 | 0.254 | 216.52 | 124 | 0.248 | 211.41 | 124 | 0.248 | 211.41 |
| 3.50 | 0.038889 | 0.001134 | 0.001180 | 114 | 0.228 | 193.24 | 109 | 0.218 | 184.76 | 115 | 0.23 | 194.93 |
| UCS (kN/m2) |  |  |  | 213.11 |  |  |  |  |  |  |  |  |

| SOIL + 6%L + 2%CCR + 1.0PW |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.005882 | 0.001134 | 0.001141 | 32 | 0.064 | 56.11 | 19 | 0.038 | 33.31 | 24 | 0.048 | 42.08 |
| 1.00 | 0.011765 | 0.001134 | 0.001148 | 57 | 0.114 | 99.35 | 43 | 0.086 | 74.95 | 51 | 0.102 | 88.89 |
| 1.50 | 0.017647 | 0.001134 | 0.001154 | 78 | 0.156 | 135.14 | 69 | 0.138 | 119.55 | 69 | 0.138 | 119.55 |
| 2.00 | 0.023529 | 0.001134 | 0.001161 | 91 | 0.182 | 156.72 | 87 | 0.174 | 149.83 | 87 | 0.174 | 149.83 |
| 2.50 | 0.029412 | 0.001134 | 0.001168 | 108 | 0.216 | 184.87 | 102 | 0.204 | 174.60 | 100 | 0.2 | 171.18 |
| 3.00 | 0.035294 | 0.001134 | 0.001175 | 116 | 0.232 | 197.36 | 119 | 0.238 | 202.47 | 114 | 0.228 | 193.96 |
| 3.50 | 0.041176 | 0.001134 | 0.001183 | 109 | 0.218 | 184.32 | 104 | 0.208 | 175.87 | 102 | 0.204 | 172.49 |
| UCS (kN/m2) |  |  |  | 197.93 |  |  |  |  |  |  |  |  |

| SOIL + 6%L + 2%CCR + 1.5PW |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.005882 | 0.001134 | 0.001141 | 20 | 0.04 | 35.07 | 25 | 0.05 | 43.83 | 18 | 0.036 | 31.56 |
| 1.00 | 0.011765 | 0.001134 | 0.001148 | 50 | 0.1 | 87.15 | 40 | 0.08 | 69.72 | 34 | 0.068 | 59.26 |
| 1.50 | 0.017647 | 0.001134 | 0.001154 | 75 | 0.15 | 129.94 | 70 | 0.14 | 121.28 | 56 | 0.112 | 97.02 |
| 2.00 | 0.023529 | 0.001134 | 0.001161 | 110 | 0.22 | 189.44 | 84 | 0.168 | 144.66 | 75 | 0.15 | 129.16 |
| 2.50 | 0.029412 | 0.001134 | 0.001168 | 100 | 0.2 | 171.18 | 99 | 0.198 | 169.47 | 93 | 0.186 | 159.20 |
| 3.00 | 0.035294 | 0.001134 | 0.001175 |  |  |  | 92 | 0.184 | 156.53 | 107 | 0.214 | 182.05 |
| 3.50 | 0.041176 | 0.001134 | 0.001183 |  |  |  |  |  |  | 98 | 0.196 | 165.72 |
| UCS (kN/m2) |  |  |  | 180.32 |  |  |  |  |  |  |  |  |

| SOIL + 6%L + 2%CCR + 2.0PW |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Penetration (mm) | Strain | Ao (m2) | Ac (m2) | Trial 1 |  |  | Trial 2 |  |  | Trial 3 |  |  |
|  |  |  |  | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) | Load DGR | Load (kN) | Stress (kN/m2) |
| 0.50 | 0.005556 | 0.001134 | 0.001140 | 16 | 0.032 | 28.06 | 18 | 0.036 | 31.57 | 14 | 0.028 | 24.55 |
| 1.00 | 0.011111 | 0.001134 | 0.001147 | 38 | 0.076 | 66.27 | 33 | 0.066 | 57.55 | 36 | 0.072 | 62.79 |
| 1.50 | 0.016667 | 0.001134 | 0.001153 | 57 | 0.114 | 98.85 | 49 | 0.098 | 84.98 | 54 | 0.108 | 93.65 |
| 2.00 | 0.022222 | 0.001134 | 0.001160 | 72 | 0.144 | 124.16 | 61 | 0.122 | 105.19 | 67 | 0.134 | 115.54 |
| 2.50 | 0.027778 | 0.001134 | 0.001166 | 84 | 0.168 | 144.03 | 78 | 0.156 | 133.74 | 76 | 0.152 | 130.32 |
| 3.00 | 0.033333 | 0.001134 | 0.001173 | 89 | 0.178 | 151.73 | 88 | 0.176 | 150.03 | 83 | 0.166 | 141.50 |
| 3.50 | 0.038889 | 0.001134 | 0.001180 | 92 | 0.184 | 155.95 | 91 | 0.182 | 154.25 | 93 | 0.186 | 157.64 |
| 4.00 | 0.044444 | 0.001134 | 0.001187 | 86 | 0.172 | 144.93 | 84 | 0.168 | 141.56 | 87 | 0.174 | 146.62 |
| UCS (kN/m2) |  |  |  | 155.95 |  |  |  |  |  |  |  |  |

CALIFORNIA BEARING RATIO

| NATURAL SOIL |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 2 | 0.17 | 3 | 0.26 |
| 1.00 | 5 | 0.43 | 7 | 0.60 |
| 1.50 | 8 | 0.68 | 13 | 1.11 |
| 2.00 | 11 | 0.94 | 17 | 1.45 |
| 2.50 | 14 | 1.19 | 21 | 1.79 |
| 3.00 | 18 | 1.53 | 24 | 2.04 |
| 3.50 | 21 | 1.79 | 27 | 2.30 |
| 4.00 | 24 | 2.04 | 30 | 2.55 |
| 4.50 | 27 | 2.30 | 32 | 2.72 |
| 5.00 | 30 | 2.55 | 35 | 2.98 |
| 5.50 | 32 | 2.72 | 37 | 3.15 |
| 6.00 | 35 | 2.98 | 40 | 3.40 |
| 6.50 | 37 | 3.15 | 43 | 3.66 |
| 7.00 | 39 | 3.32 | 45 | 3.83 |
| 7.50 | 43 | 3.66 | 47 | 4.00 |

| 6% LIME |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 2 | 0.17 | 3 | 0.26 |
| 1.00 | 6 | 0.51 | 9 | 0.77 |
| 1.50 | 9 | 0.77 | 15 | 1.28 |
| 2.00 | 12 | 1.02 | 18 | 1.53 |
| 2.50 | 15 | 1.28 | 21 | 1.79 |
| 3.00 | 20 | 1.70 | 24 | 2.04 |
| 3.50 | 23 | 1.96 | 27 | 2.30 |
| 4.00 | 25 | 2.13 | 31 | 2.64 |
| 4.50 | 28 | 2.38 | 34 | 2.89 |
| 5.00 | 31 | 2.64 | 36 | 3.06 |
| 5.50 | 34 | 2.89 | 38 | 3.23 |
| 6.00 | 37 | 3.15 | 40 | 3.40 |
| 6.50 | 40 | 3.40 | 42 | 3.57 |
| 7.00 | 42 | 3.57 | 45 | 3.83 |
| 7.50 | 45 | 3.83 | 47 | 4.00 |

| 6% LIME + 1%CCR |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 3 | 0.26 | 2 | 0.17 |
| 1.00 | 5 | 0.43 | 8 | 0.68 |
| 1.50 | 8 | 0.68 | 14 | 1.19 |
| 2.00 | 12 | 1.02 | 19 | 1.62 |
| 2.50 | 16 | 1.36 | 23 | 1.96 |
| 3.00 | 19 | 1.62 | 25 | 2.13 |
| 3.50 | 24 | 2.04 | 28 | 2.38 |
| 4.00 | 27 | 2.30 | 30 | 2.55 |
| 4.50 | 31 | 2.64 | 32 | 2.72 |
| 5.00 | 35 | 2.98 | 34 | 2.89 |
| 5.50 | 37 | 3.15 | 37 | 3.15 |
| 6.00 | 40 | 3.40 | 39 | 3.32 |
| 6.50 | 42 | 3.57 | 43 | 3.66 |
| 7.00 | 45 | 3.83 | 45 | 3.83 |
| 7.50 | 47 | 4.00 | 48 | 4.08 |

| 6% LIME + 2%CCR |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 4 | 0.34 | 3 | 0.26 |
| 1.00 | 7 | 0.60 | 8 | 0.68 |
| 1.50 | 12 | 1.02 | 11 | 0.94 |
| 2.00 | 15 | 1.28 | 15 | 1.28 |
| 2.50 | 18 | 1.53 | 19 | 1.62 |
| 3.00 | 20 | 1.70 | 23 | 1.96 |
| 3.50 | 23 | 1.96 | 27 | 2.30 |
| 4.00 | 25 | 2.13 | 30 | 2.55 |
| 4.50 | 28 | 2.38 | 32 | 2.72 |
| 5.00 | 31 | 2.64 | 35 | 2.98 |
| 5.50 | 34 | 2.89 | 37 | 3.15 |
| 6.00 | 37 | 3.15 | 40 | 3.40 |
| 6.50 | 39 | 3.32 | 42 | 3.57 |
| 7.00 | 41 | 3.49 | 45 | 3.83 |
| 7.50 | 44 | 3.74 | 46 | 3.91 |

| 6% LIME + 1%CCR + 0.5PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 4 | 0.34 | 3 | 0.26 |
| 1.00 | 7 | 0.60 | 7 | 0.60 |
| 1.50 | 10 | 0.85 | 12 | 1.02 |
| 2.00 | 15 | 1.28 | 17 | 1.45 |
| 2.50 | 19 | 1.62 | 23 | 1.96 |
| 3.00 | 22 | 1.87 | 26 | 2.21 |
| 3.50 | 25 | 2.13 | 29 | 2.47 |
| 4.00 | 28 | 2.38 | 33 | 2.81 |
| 4.50 | 32 | 2.72 | 36 | 3.06 |
| 5.00 | 34 | 2.89 | 39 | 3.32 |
| 5.50 | 37 | 3.15 | 41 | 3.49 |
| 6.00 | 39 | 3.32 | 43 | 3.66 |
| 6.50 | 42 | 3.57 | 46 | 3.91 |
| 7.00 | 45 | 3.83 | 48 | 4.08 |
| 7.50 | 48 | 4.08 | 50 | 4.25 |

| 6% LIME + 1%CCR + 1.0PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 3 | 0.26 | 4 | 0.34 |
| 1.00 | 7 | 0.60 | 8 | 0.68 |
| 1.50 | 12 | 1.02 | 11 | 0.94 |
| 2.00 | 15 | 1.28 | 15 | 1.28 |
| 2.50 | 19 | 1.62 | 20 | 1.70 |
| 3.00 | 22 | 1.87 | 24 | 2.04 |
| 3.50 | 26 | 2.21 | 27 | 2.30 |
| 4.00 | 30 | 2.55 | 31 | 2.64 |
| 4.50 | 34 | 2.89 | 35 | 2.98 |
| 5.00 | 38 | 3.23 | 39 | 3.32 |
| 5.50 | 41 | 3.49 | 43 | 3.66 |
| 6.00 | 45 | 3.83 | 45 | 3.83 |
| 6.50 | 47 | 4.00 | 48 | 4.08 |
| 7.00 | 50 | 4.25 | 51 | 4.34 |
| 7.50 | 52 | 4.42 | 54 | 4.59 |

| 6% LIME + 1%CCR + 1.5PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 3 | 0.26 | 4 | 0.34 |
| 1.00 | 7 | 0.60 | 9 | 0.77 |
| 1.50 | 11 | 0.94 | 12 | 1.02 |
| 2.00 | 14 | 1.19 | 16 | 1.36 |
| 2.50 | 18 | 1.53 | 21 | 1.79 |
| 3.00 | 21 | 1.79 | 25 | 2.13 |
| 3.50 | 25 | 2.13 | 28 | 2.38 |
| 4.00 | 28 | 2.38 | 31 | 2.64 |
| 4.50 | 32 | 2.72 | 34 | 2.89 |
| 5.00 | 36 | 3.06 | 37 | 3.15 |
| 5.50 | 39 | 3.32 | 40 | 3.40 |
| 6.00 | 41 | 3.49 | 43 | 3.66 |
| 6.50 | 43 | 3.66 | 45 | 3.83 |
| 7.00 | 46 | 3.91 | 48 | 4.08 |
| 7.50 | 48 | 4.08 | 50 | 4.25 |

| 6% LIME + 1%CCR + 2.0PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 2 | 0.17 | 3 | 0.26 |
| 1.00 | 6 | 0.51 | 7 | 0.60 |
| 1.50 | 10 | 0.85 | 11 | 0.94 |
| 2.00 | 13 | 1.11 | 15 | 1.28 |
| 2.50 | 16 | 1.36 | 19 | 1.62 |
| 3.00 | 19 | 1.62 | 23 | 1.96 |
| 3.50 | 22 | 1.87 | 27 | 2.30 |
| 4.00 | 26 | 2.21 | 31 | 2.64 |
| 4.50 | 29 | 2.47 | 34 | 2.89 |
| 5.00 | 32 | 2.72 | 37 | 3.15 |
| 5.50 | 35 | 2.98 | 39 | 3.32 |
| 6.00 | 37 | 3.15 | 42 | 3.57 |
| 6.50 | 40 | 3.40 | 45 | 3.83 |
| 7.00 | 42 | 3.57 | 48 | 4.08 |
| 7.50 | 45 | 3.83 | 50 | 4.25 |

| 6% LIME + 2%CCR + 0.5PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 3 | 0.26 | 5 | 0.43 |
| 1.00 | 8 | 0.68 | 8 | 0.68 |
| 1.50 | 12 | 1.02 | 13 | 1.11 |
| 2.00 | 17 | 1.45 | 17 | 1.45 |
| 2.50 | 21 | 1.79 | 21 | 1.79 |
| 3.00 | 25 | 2.13 | 24 | 2.04 |
| 3.50 | 28 | 2.38 | 27 | 2.30 |
| 4.00 | 31 | 2.64 | 30 | 2.55 |
| 4.50 | 34 | 2.89 | 33 | 2.81 |
| 5.00 | 36 | 3.06 | 35 | 2.98 |
| 5.50 | 40 | 3.40 | 37 | 3.15 |
| 6.00 | 43 | 3.66 | 40 | 3.40 |
| 6.50 | 45 | 3.83 | 43 | 3.66 |
| 7.00 | 47 | 4.00 | 46 | 3.91 |
| 7.50 | 50 | 4.25 | 48 | 4.08 |

| 6% LIME + 2%CCR + 1.0PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 3 | 0.26 | 5 | 0.43 |
| 1.00 | 6 | 0.51 | 8 | 0.68 |
| 1.50 | 10 | 0.85 | 12 | 1.02 |
| 2.00 | 14 | 1.19 | 16 | 1.36 |
| 2.50 | 17 | 1.45 | 20 | 1.70 |
| 3.00 | 20 | 1.70 | 24 | 2.04 |
| 3.50 | 24 | 2.04 | 27 | 2.30 |
| 4.00 | 28 | 2.38 | 30 | 2.55 |
| 4.50 | 32 | 2.72 | 34 | 2.89 |
| 5.00 | 36 | 3.06 | 37 | 3.15 |
| 5.50 | 39 | 3.32 | 39 | 3.32 |
| 6.00 | 42 | 3.57 | 41 | 3.49 |
| 6.50 | 45 | 3.83 | 44 | 3.74 |
| 7.00 | 47 | 4.00 | 46 | 3.91 |
| 7.50 | 49 | 4.17 | 49 | 4.17 |

| 6% LIME + 2%CCR + 1.5PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 3 | 0.26 | 5 | 0.43 |
| 1.00 | 7 | 0.60 | 8 | 0.68 |
| 1.50 | 11 | 0.94 | 13 | 1.11 |
| 2.00 | 16 | 1.36 | 18 | 1.53 |
| 2.50 | 20 | 1.70 | 22 | 1.87 |
| 3.00 | 24 | 2.04 | 26 | 2.21 |
| 3.50 | 26 | 2.21 | 30 | 2.55 |
| 4.00 | 29 | 2.47 | 33 | 2.81 |
| 4.50 | 31 | 2.64 | 37 | 3.15 |
| 5.00 | 34 | 2.89 | 40 | 3.40 |
| 5.50 | 37 | 3.15 | 43 | 3.66 |
| 6.00 | 40 | 3.40 | 45 | 3.83 |
| 6.50 | 42 | 3.57 | 48 | 4.08 |
| 7.00 | 45 | 3.83 | 50 | 4.25 |
| 7.50 | 48 | 4.08 | 52 | 4.42 |

| 6% LIME + 2%CCR + 2.0PW |  |  |  |  |
| --- | --- | --- | --- | --- |
| Penetration (mm) | TOP |  | BOTTOM |  |
|  | Dial Gauge Reading | Force (kN) | Dial Gauge Reading | Force (kN) |
| 0.00 | 0 | 0.00 | 0 | 0.00 |
| 0.50 | 4 | 0.34 | 3 | 0.26 |
| 1.00 | 9 | 0.77 | 7 | 0.60 |
| 1.50 | 13 | 1.11 | 12 | 1.02 |
| 2.00 | 17 | 1.45 | 15 | 1.28 |
| 2.50 | 21 | 1.79 | 18 | 1.53 |
| 3.00 | 25 | 2.13 | 21 | 1.79 |
| 3.50 | 28 | 2.38 | 24 | 2.04 |
| 4.00 | 31 | 2.64 | 28 | 2.38 |
| 4.50 | 33 | 2.81 | 30 | 2.55 |
| 5.00 | 36 | 3.06 | 33 | 2.81 |
| 5.50 | 39 | 3.32 | 36 | 3.06 |
| 6.00 | 42 | 3.57 | 38 | 3.23 |
| 6.50 | 45 | 3.83 | 41 | 3.49 |
| 7.00 | 48 | 4.08 | 43 | 3.66 |
| 7.50 | 50 | 4.25 | 46 | 3.91 |

CBR= Test LoadStandard Load×100%

Standard load at 2.50mm penetration = 13.24kN, at 5.0mm penetration = 19.96kN.0

| S/N | SAMPLE MIX | SAMPLE DESCRIPTION |
| --- | --- | --- |
| 1. | SOIL + 6% L | L6 |
| 2. | SOIL + 6%L +1% CCR | L6-C1 |
| 3. | SOIL + 6%L +1% CCR + 0.5%PW | L6-C1-P0.5 |
| 4. | SOIL + 6%L +1% CCR + 1%PW | L6-C1-P1 |
| 5. | SOIL + 6%L +1% CCR + 1.5%PW | L6-C1-P1.5 |
| 6. | SOIL + 6%L +1% CCR + 2%PW | L6-C1-P2 |
| 7. | SOIL + 6%L + 2%CCR | L6-C2 |
| 8. | SOIL + 6%L +2% CCR + 0.5%PW | L6-C2-P0.5 |
| 9. | SOIL + 6%L +2% CCR + 1%PW | L6-C2-P1 |
| 10. | SOIL + 6%L +2% CCR + 1.5%PW | L6-C2-P1.5 |
| 11. | SOIL + 6%L +2% CCR + 2%PW | L6-C2-P2 |

| SAMPLE | LL | PL | LS | PI | MDD | OMC | UCS | CBR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SOIL | 56.5 | 31.18 | 7.86 | 25.32 | 1781 | 15 | 147.53 | 14.23 |
| L6 | 59.60 | 48.69 | 6.43 | 10.91 | 1821 | 20.60 | 176.46 | 14.31 |
| L6-C1 | 77.10 | 49.43 | 7.97 | 27.67 | 1760 | 19.20 | 196.19 | 14.87 |
| L6-C1-P0.5 | 77.50 | 51.55 | 7.86 | 26.75 | 1802 | 19.20 | 185.04 | 15.72 |
| L6-C1-P1 | 77.70 | 52.65 | 7.86 | 25.05 | 1769 | 18.30 | 183.17 | 14.74 |
| L6-C1-P1.5 | 81.10 | 52.92 | 7.25 | 28.18 | 1720 | 16.20 | 169.75 | 14.65 |
| L6-C1-P2 | 82.85 | 50.60 | 7.14 | 32.25 | 1721 | 21.60 | 160.17 | 14.01 |
| L6-C2 | 76.50 | 48.08 | 7.86 | 28.42 | 1748 | 19.8 | 206.08 | 13.59 |
| L6-C2-P0.5 | 79.35 | 53.73 | 7.14 | 25.62 | 1701 | 17.50 | 213.11 | 14.43 |
| L6-C2-P1 | 77.00 | 53.53 | 8.63 | 23.47 | 1723 | 16.00 | 197.93 | 14.55 |
| L6-C2-P1.5 | 81.00 | 53.18 | 7.97 | 27.82 | 1713 | 16.60 | 180.32 | 15.58 |
| L6-C2-P2 | 83.15 | 52.89 | 6.98 | 30.26 | 1677 | 21.85 | 155.95 | 14.43 |